## Slide 1: Low Carbon Cements and Concrete in Modern Construction
www.gaiaengineering.com
Gaia Engineering
A John W Harrison Managing Director TecEco Pty. Ltd. and self funded private researcher.
www.tececo.com www.gaiaengineering.com

## Slide 2: A Brief History of How Life on Earth Controls the Climate
The first life on earth began about 3.5 billion years ago.
The first oxygen was released by cyanobacteria.
  Initially consumed by free iron in the oceans and precipitated to form iron ore.
  Then started forming our atmosphere about 2.4 billion years ago.
  Chloroplasts in plants evolved from them.
  Life has controlled climate ever since

## Slide 3: Paleoclimate
The Great Oxygenation
Free Oxygen

## Slide 4: The Industrial Revolution – Machines

## Slide 5: The Result - A Rising Rate of Warming

## Slide 6: Net Atmospheric Emissions
For Portland Cement:
Using the latest figures available which are from the Chinese Ministry of Environment Protection (MEP 2011) and they agree with the numbers I have from our LCA model.
877 kg of CO2 are emitted for every tonne of Portland cement clinker produced, 820 kg from direct processes and 57 kg from indirect sources (the burning of coal for the electric power needed). MEP also estimates that waste heat recycling in the industry saves 16 kg CO2 emissions – making 861 kg for each tonne of cement produced This is close to the figure TecEco have in their LCA downloadable under Downloads\Tools on the TecEco web site. Using these figures, the production of 3.4 billion tonnes cement would thus lead to emissions of 2.9 billion tonnes CO2.
The current contribution of cement production globally is therefore 2.9/33 x 100%, or 8.8%.
For Global Anthropogenic Emissions:
According to recent research published in Nature, carbon emissions from burning fossil fuels and producing cement reached 9.1±0.5 Pg Carbon (9.1 billion tonnes carbon, or 33 billion tonnes carbon dioxide) in 2011.
Source: Peters, G.P., Marland, G., Le Quere, C., Boden, T., Canadell, J.G. and Raupach, M.R. 2012. Rapid growth in CO2 emissions after the 2008-2009 global financial crisis, Nature Climate Change, 2: 2-4

## Slide 7: The Techno Process
Extract, Process, Build, & Manufacture, Use, Dispose
Underlying Molecular Flows
Extract
Methane NOX & SOX Heavy Metals CO2 etc.
Embodied & Process Energy
Process, Build & Manufacture
NOX & SOX
Heavy Metals CO2 etc.
Embodied & Process Energy
Use
NOX & SOX
Heavy Metals CO2 etc.
Lifetime Energy
Dispose or Waste
Methane NOX & SOX
Heavy Metals CO2 etc.
Process Energy
These are the releases and impacts we look at with LCA and LCCA

## Slide 8: A Doom Cycle or Environmental Catastrophe Waiting to Happen?
Global Warming
Aircon
Greater Energy Use
“We have to find a way through this debacle”

## Slide 9: Wouldn't it be Great if we Could Add Technical Value to Wastes.
The technical paradigm defines what is or is not a resource!
Reactive magnesia as an additive to Portland cement that improves polar bonding and sticks to just about any waste.
Wastes have physical and chemical properties that add value in composites!

## Slide 10: We Can Add Technical Value to Wastes – Including CO2 – and Improve Concrete as a Material doing so!
The Indian Culture is the right base to start from but we need to dig into our minds

## Slide 11: By Adding Value to Wastes –Jobs are Created. The Lifetime as well and Embodied Energy Performance of Concretes can be Improved.
Many people can live much better if we can find ways of technically using wastes for their physical and chemical properties thereby turning them into resources and in so doing adding to their value.
We can do this and reactive magnesia (rMgO) is the technical key but it needs to be much cheaper.

## Slide 12: Huge Potential for Doing it Better
All that is grey is not great.
  We not only need to think not only whole of concrete but expand our thinking to all composites utilising any mineral binder.
The rising cost of energy will determine that
  The future is for mineral composites
    In which wastes including CO2 add useful properties such as fire resistance, tensile strength, thermal capacity or resistance.
    Cementitious composites will be important if we are to reduce lifetime energies as required by the IEA Cement 2050 Roadmap.

## Slide 13: Embodied Energy and Emissions over Time
13 Source: Slide in presentation by Prof Roland Pellenq, MIT Concrete Sustainability Hub
The properties of materials chosen have a big influence on the lifetime or operational energies of buildings.

## Slide 14: Conclusions from Introductory Slides.
There are some significant problems facing humanity including climate change, ocean acidity and food shortages, land degradation and water pollution by wastes.
At the 2007 “Driving CO2 Reduction” National Conference held in Melbourne on 13 & 14 September 2007 M K Singh stood up and said “I want the cement industry to be the saviour of the world”.
  Cementitious composites can be and those in the industry who take on this challenge will succeed.
  We must however think outside the square and develop new technical paradigms.
A fundamental truism of industrial ecology is that the technology paradigm defines what is or is not a resource.
A broader range of cementitious composites will be required if we are to dramatically reduce lifetime energies of buildings
There is a way to profitably capture and store CO2 – more to follow

## Slide 15: Concrete Today
The mineral composite we build with.
Next to water the most used.
  Global cement production was 3.4 billion tonnes in 2011 and the concrete produced with it roughly 28 billion tonnes.
  The annual carbon emissions from the cement in this huge material flow amount to roughly 2.9 billion tonnes of carbon dioxide, or 8.8%1 of total anthropogenic carbon emissions.
  China and India between them are now consuming 40 times more cement and concrete than the USA. India currently produces around 210 million tonnes of cement, second to China at around 2 billion tonnes.2
1 MEP. Technical Requirements for Environmental Labeling Products: Low-carbon Cement (Discussion Paper) [Internet]. Ministry of Environment Protection, China; 2012. Available from: http://www.mep.gov.cn/gkml/hbb/bgth/201112/W020111208396803781008.pdf (in Chinese).
2 USGS. Mineral Commodity Summary - Cement [Internet]. 2012, (2012):Available from: http://minerals.usgs.gov/minerals/pubs/commodity/cement/mcs-2012-cemen.pdf.

## Slide 16: Construction and Concrete
Buildings account for ~40% of the materials and ~33% of the energy consumed by the world economy. 3
  7 billion M3 per annum 2
  5% - 10% of CO2 emissions depending on the authority.
Concrete infrastructure expenditure a huge investment for governments at all levels but has high multipliers in an economy.
A cost cutting volume business model for many players in the supply chain. Arguably models should be innovation based.
Concrete production and use a good indicator or the state of a country’s economy.
Already one of the most environmentally friendly building materials – significant improvements are possible however.
3 Rees, W. E. (1999). The Built Environment and Ecosphere: A Global Perspective.
Building Research and Information. British Columbia, William E Rees. 27: 206-220
4 Wallenvik, Olafur, Carbon Footprint of High Performance Versus Conventional Vibrated Concrete

## Slide 17: We Can Recycle Safely and Profitably in Concrete !
Cementitious composites are a safe repository for wastes provided we regulate the pH for the minimum solubility of heavy metals.
  The use of rMgO in hydraulic cement compositions achieves this.
  Somebody please tell the EPA in the US!
Waste CO2 and waste magnesium ions can be combined to form magnesium carbonates which can be the foundation of manufactured aggregates that can be combined with vast volumes of other wastes because of their polar nature.
I use the word “can” because all my company needs is money.

## Slide 18: The Good News!
There is a solution to global warming, salinity and many other global problems and it is potentially very profitable.
TecEco Gaia Engineering utilises the huge flow of concrete to create an enormous sink for CO2 and other wastes in aggregates and I will explain this as I go through the options and issues for cement and concrete in modern construction.
The IEA Cement 2050 Roadmap mentions carbon capture and storage and significant reductions in operational or lifetime energies.
  Our Gaia Engineering is a technically feasible profitable way forward.

## Slide 19: Drivers for Innovative Change
Stakeholder demands for greater sustainability
  Brundtland definition and triple bottom line.
  The precautionary principle & intergenerational equity
  Every improvement counts but paradigm improvements really matter – If implemented!, but
  Quick fixes = paradigm changes
Economic Cost Benefit given
  Rapidly rising energy costs
  Carbon taxes
    Construction activities contribute over 35% of total global CO2 emissions3 so carbon taxes will have a big impact.
> Sustainability can deliver > profit.
Competition – Leed, the Green Building Council etc.
Improved technical understanding and practice
Government research and development as well as procurement policies
The need to change!
3UNEP (2001). Energy and Cities: Sustainable Building and Construction Summary of Main Issues,
IETC Side Event at UNEP Governing Council, Nairobi, Kenya, UNEP.
Legislation and control will not get us there. Changing technical paradigms will.

## Slide 20: Better more cost effective concrete is more sustainable
Concrete is not a perfect material yet. E.g. It shrinks, it cracks, it is not as durable as we would like and has a limited range of properties.
  See how we fix many these issues in Part 2 - the section on reactive MgO
Better concrete is not hard to make and there are huge opportunities for change
Improvements through innovation = Sustainable profit!
Increase in demand/price ratio for sustainability due to educationally induced cultural drift.
#
$
Demand
Supply
Increase in supply/price ratio for more sustainable products due to innovative changes in the technical paradigm.
Equilibrium shift
Sustainable profit
ECONOMICS
Paradigm
shifts ~ Lots
of little shifts!

## Slide 21: Predicted Global Cement Demand, Emissions and Compositional Change
1 Quillin K. Low-CO2 Cements based on Calcium Sulfoaluminate [Internet]. Available from: http://www.soci.org/News/~/media/Files/Conference%20Downloads/Low%20Carbon%20Cements%20Nov%2010/Sulphoaluminate_Cements_Keith_Quillin_R.ashx
According to the British Research Establishment (BRE) we cannot address de-carbonation without changing the composition of cement and fuel derived emissions will diminish slowly for purely economic reasons 1
The BRE may be wrong however. The composition of cement does not have change so much as the composition of concrete. Cement is only around 10% of concrete. At TecEco we believe Portland cement is here to stay if rectified the way we say!

## Slide 22: Mehta’s Triangle
Mehta summarised some of the techniques for dematerialisation1 but did not consider the effect on lifetime energies
1 MEHTA PK. Global Concrete Industry Sustainability. Concrete International. 2009, Vol 31(2):4.

## Slide 23: Ways to make Cement and Concrete More Sustainable.
Option | Description | Players | Drivers | Barriers | Standards & Guides
Alternative Binders | Numerous and described in Table 2 - Future Binder Contenders with Differentiated Supply Chain Options | Scientists (Cement Chemists) | Sustainability and profit. | Conservatism, out dated software. Prescription standards and approvals systems (see http://www.tececo.com/sustainability.permissions_rewards.php.) | A few guides and draft standards (e.g. with Geopolymers)
CO2 Capture during Manufacture | Reduce process emissions. Cements that involve calcination can be made without releases. | Scientists. TecEco and Calix. | Sustainability, carbon taxes. | Inability to think laterally. Fear of change | Common sense!
Replacement of Portland cement by Limestone | Blending with Limestone with cement to reduce net emissions has met with some success and is now incorporated into many standards. There are however issues. | Cement technol- ogists | Economic cost/benefit, sustainability, Leed, GBC, r & d & procurement Policies. | Buyer hesitancy. | New standards emerging because industry driven.

## Slide 24: Ways to make Cement and Concrete More Sustainable.
Option | Description | Players | Drivers | Barriers | Standards & Guides
Replacement of cement by SCM’s | Blended cements that contain a high volume of replacement materials (SCM’s) such as fly ash, slag cement (gbfs), pozzolans, silica fume, rice husk ash etc. High replacement cement concretes often have improved properties such as rheology, less shrinkage, greater durability etc. The use of reactive MgO makes the use of higher proportions of SCM’s possible. | Cement technol ogists | Economic cost/benefit, sustainability, Leed, GBC, R & D & procurement Policies. | Conservatism, out dated software. Prescription standards and approvals systems (see http://www.tececo.com/sustainability.permissions_rewards.php.) | Mix design methods. LCA & LCCA. New better software.
Dematerial-isation | Innovative architecture and engineering. More durable concretes. KgCO2e/MPa | Architects & Engineers | Economic cost/benefit, sustainability, Leed, GBC, r & d & procurement Policies. | Prescription standards and approvals systems (see http://www.tececo.com/sustainability.permissions_rewards.php.) | Design codes, LCA & LCCA

## Slide 25: Ways to make Cement and Concrete More Sustainable.
Option | Description | Players | Drivers | Barriers | Standards & Guides
Mix Optimisation | Appropriate particle packing, better admixtures and use of Brucite hydrates to release water for more complete hydration | Cement technologists | Economic cost/benefit, sustainability. | Conservatism, inappropriate software. Prescription standards and approvals systems (see http://www.tececo.com/sustainability.permissions_rewards.php.) | Mix design methods. LCA & LCCA. New better software.
Product Differentiation and Specialisation | Mineral composites other than concrete with just stone aggregate can improve sustainability. E.g. composites with a high “R” value | Materials scientists | Economic cost/benefit | Inability to think outside the box. Fear of change | Standards, LCA & LCCA
Changing the emphasis | An emphasis other than on the binder to improve sustainability. E.g. Use of synthetic carbonate aggregate. | Scientists | Sustainability, economic cost/benefit. Technical merit | Inability to think outside the box. Fear of change. Technical issues (?). | Common sense!

## Slide 26: Ways to make Cement and Concrete More Sustainable.
Option | Description | Players | Drivers | Barriers | Standards & Guides
The Right Business Model | Although not a technical matter the right business model is essential for progress to be made. | Consultants | Profitability in a changing business environment | Conservatism, standards and legislative environment. | 
The Right Framework to Operate in | Legislative restrictions and standards throughout the world are prescriptive in nature and this and a lack of training is holding back innovation | Consultants | The need to change | Conservatism, inability or unwillingness to change. | 
 | Critical
 | Important
 | Relevant
 | A Furphy

## Slide 27: Alternative Binders (A Summary)
Hydraulic Cements
  Slag-lime or slag – Portland Cement (PC) cements
  Calcium sulfoaluminate cements & belite calcium sulfoaluminate cements
  Calcium aluminate cements
  Belite cements
  Reactive magnesia blended with other hydraulic cements and Supplementary Cementitious Materials (SCM’s)
Chemical Cements
  Magnesium Phosphate Cements

## Slide 28: Alternative Binders
Carbonating Cements
  Reactive Magnesia Based Carbonating Binders
  Lime Based Carbonating Binders
Other Cements
  Geopolymers
  Sialites
Please see pages 7 - 9 and Table 2 in the paper “LOW CARBON CEMENTS AND CONCRETE IN MODERN CONSTRUCTION” UKIERI Conference, Jalandhar, India 5 – 8 March 2013.
for advantages, limitations, associated energies, supply chain options and more detail !
The LCA spreadsheet we used to calculate energies and emissions is on our web sites covering hydraulic binders and soon there will be a LCCA!

## Slide 29: Alternative Manufacturing Processes
So far the industry response has mostly been to:
  Modernise and upgrade plant
    Convert wet to dry plant processes
    Convert shaft to rotary kilns
    Install preheating, more efficient burners etc.
    Improve grinding and other efficiencies.
  Burn cheaper waste fuels. Burning waste materials with high calorific value including timber, tyres, solvents, waste oil, animal fats, carbon waste from the aluminium industry1 etc. has met with opposition in some countries because of the associated pollution.
  Reduce kiln temperatures and adjust the composition of cement accordingly with more aluminates and less alite2.
1Mcgrath T M Sustainable cement and concrete. Concrete in Australia. 2012, 38(1):15‑15.
2Pers comm. WA (Tony) Thomas – Chief Engineer Concrete, Boral Construction Materials

## Slide 30: Manufacturing taking Advantage of full Thermodynamic Cycles
The manufacture and use of Portland cement does not involve a full thermodynamic cycle.
  there is therefore little point in splitting the process into the endothermic and exothermic sub processes with one or two exceptions such as the manufacture of Syngas1.
There is however a great deal of merit in capturing CO2 during manufacture and our Gaia Engineering focusses on how to do this profitably in a sustainable way.
1 Dr Sheila Devasahayam at the SMaRT Centre, School of Materials Science and Engineering, The University Of New South Wales, is researching pyroprocessing CaCO3 with an additive to produce Syngas

## Slide 31: Options for Portland Cement Manufacture
1450 0C

## Slide 32: Options for Carbonation Binders like TecEco Eco-Cement are Greater

## Slide 33: Capture During Manufacture
Significant sequestration can be achieved with capture of CO2 from cement and lime kilns which are a concentrated point source.
  Recognised as important by the IEA Cement 2050 Roadmap.
  The problem, which has not been solved yet for any form of sequestration, is what to do with the enormous volume of CO2 produced
  TecEco have developed the N-Mg sub-process of Gaia Engineering that will profitably sequester huge amounts of CO2 as synthetic carbonate that can be used as aggregate with or without other wastes and / or as feedstock to make rMgO for our patented cements.

## Slide 34: Gaia Engineering and the new TecEco “N-Mg” process to profitably sequester massive tonnages of CO2 in the built environment as synthetic carbonate concretes.
www.gaiaengineering.com
Gaia Engineering
This presentation is available for download on our web sites shown below
A Solution to Global Warming

## Slide 35: Gaia Engineering
We realised that the answer to the worlds problems lay in an industrial ecology that utilised wastes including CO2 and bitterns, de-sal waste water or oil process water to create valuable products for the worlds biggest market which is building and construction.
By including the manufacture of not only TecEco patented cements but aggregates in the concept of synthetic carbonate built environment a solution to global warming can be achieved.
TecEco have changed the technical paradigm in favour of making CO2 and other wastes resources

## Slide 36: Gaia Engineering Summary
The real game changer and pinnacle of industrial ecology is our N-Mg sub process of Gaia Engineering that will produce large quantities of nesquehonite (MgCO3.3H2O) from waste magnesium cations such as found in oil process water, bitterns and waste from de-sal plants and if this source runs out then from any brine containing Mg++(step 1).
Nesquehonite can then be calcined in our Tec-Kiln without releases (step 2) to make rMgO and the CO2 fed back into the process (step 1) to precipitate more nesquehonite.
The rMgO is then used as a binder to agglomerate massive amounts of nesquehonite with or without other wastes such as fly ash to make synthetic carbonate aggregate or in TecEco Eco-Cements where it re carbonates (step 3).
www.gaiaengineering.com
Gaia Engineering

## Slide 37: The Concept of a Carbonate Built Environment
John Harrison from TecEco has for many years been advocating the carbonate built environment solution to global warming
13th July 2002 – Fred Pearce in New Scientist about TecEco magnesium cement technology:
“THERE is a way to make our city streets as green as the Amazon rainforest. Almost every aspect of the built environment, from bridges to factories to tower blocks, and from roads to sea walls, could be turned into structures that soak up carbon dioxide- the main greenhouse gas behind global warming. All we need to do is change the way we make cement.” (By including aggregates and considering concrete as a whole the potential for sequestration is much greater.)
All we have to do is change the way we do things and do what a big old tree does – make our homes out of CO2.

## Slide 38: The Sequestration Potential for Synthetic Carbonates in Concretes
Chart: 
Source USGS: Cement Pages
Assumptions |  | 
Tec-Cement concrete with synthetic magnesium carbonate aggregate |  | 
Percentage by weight of cement in concrete | 12.00% | 
Percentage by weight of rMgO in Tec-Cement | 9% | 
Percentage by weight Ca(OH)2 in cement | 29% | 
% of Ca(OH)2 in concrete that carbonates | 10.00% | 
Proportion cement that is fly ash and/or GBFS | 20% | 
1 tonne Portland Cement | 0.867 | Tonnes CO2
Proportion concrete that is aggregate | 80.0% | 
CO2 captured in 1 tonne aggregate | 1.084 | Tonnes CO2
Net CO2 sequestration 1 tonne rMgO (N-Mg route, 1 complete recycle) | 1.794 | Tonnes CO2
CO2 captured hydration and carbonation of 1 tonne CaO (in PC) | 0.785 | Tonnes CO2
Tonnes

## Slide 39: The Viability of Sequestration Technologies
A viable Sequestration Technology must be:
  Simple
  Scalable
  Have low up front capital costs (post combustion)
  Low environmental impacts
  Produce saleable products with insatiable markets
  Easily implemented and
  Deployable over a wide geographical area
It should also ideally
  Be industrially symbiotic and
  address one or more other major problems facing the planet.

## Slide 40: ECRA Concepts – Not Viable
No efficient means of capture, no viable means of storage. Oxyfuel combustion ridiculously expensive
http://cement.mineralproducts.org/special_features/a_carbon_capture_and_storage.php

## Slide 41: Viability of Gaia Engineering
Gaia Engineering satisfies all the criteria set on the previous slide and is a magnificent example of industrial ecology in action.
It can utilise many waste streams and nothing is produced that cannot be utilised.
It is the only potentially profitable solution.
There are environmental advantages not impacts.

## Slide 42: Gaia Engineering
The process is scalable and can use intermittent energy from non fossil fuel sources. It can add value using the energy available without having to store it. Gaia Engineering can produce synthetic carbonate concrete and building products with it.
The built environment represents what we do on this planet and is a large insatiable market for synthetic carbonate building products at the right price.
Gaia Engineering addresses other problems such as waste utilization and the production of cleaner water.

## Slide 43: Why is Gaia Engineering Low Cost?
Gaia Engineering has much lower costs than older processes such as developed by NETL some years ago because:
There are less process steps.
  Gaia Engineering involves no mining, no transport, no grinding and no need to process silicate.
No wastes are produced that cannot be used or recycled.
The output from the process is saleable.
A draft LCCA will soon be on our web sites

## Slide 44: Natural Carbon Sinks
Carbon Sinks and Anthropogenic Actual and Predicted Consumption of Carbon
Modified from Figure 2 in Ziock, H. J. and D. P. Harrison. "Zero Emission Coal Power, a New Concept." from http://www.netl.doe.gov/publications/proceedings/01/carbon_seq/2b2.pdf. by the inclusion of a bar to represent sedimentary sinks.
Over the last 4 billion years CO2 produced by animals, volcanos and other sources has been sequestered in carbonate sediments such as limestone.

## Slide 45: Sequestration Permanence
Data from Figure 2 in Ziock, H. J. and D. P. Harrison. "Zero Emission Coal Power, a New Concept." from http://www.netl.doe.gov/publications/proceedings/01/carbon_seq/2b2.pdf. by the inclusion of a bar to represent sedimentary sinks.
Carbonate sediments such as limestone are permanent sinks.

## Slide 46: What Carbonate?
The following table lists principal metal oxides of Earth's Crust. Theoretically up to 22% of this mineral mass is able to form carbonates.
Table Source: http://en.wikipedia.org/wiki/Carbon_sequestration
Oxide | Percent of Crust | Carbonate | Enthalpy change (kJ/mol) | Comment
SiO2 | 59.71 |  |  | Too difficult
Al2O3 | 15.41 |  |  | Too difficult
CaO | 4.90 | CaCO3 | -179 | Feasible
rMgO | 4.36 | MgCO3 | -117 | Feasible
Na2O | 3.55 | Na2CO3 |  | Too soluble
FeO | 3.52 | FeCO3 |  | Too difficult
K2O | 2.80 | K2CO3 |  | Too soluble
Fe2O3 | 2.63 | FeCO3 |  | Too difficult
 | 21.76 | All Carbonates |  | 

## Slide 47: Magnesium Carbonates
Seawater Reference Data | g/l H20 | Cation radius (pm)
Chloride (Cl--) | 19 | 167
Sodium (Na+) | 10.5 | 116
Sulfate (S04--) | 2.7 | ?
Magnesium (Mg++) | 1.29 | 86
Calcium (Ca++) | 0.412 | 114
Potassium (K+) | 0.399 | 152
Because of the low molecular weight of magnesium, it is ideal for scrubbing CO2 out of the air and sequestering the gas into the built environment:
More CO2 is captured than in calcium systems as the calculations below show.
At 2.09% of the crust magnesium is the 8th most abundant element
Sea-water contains 1.29 g/l compared to calcium at .412 g/l. Many brines contain much more.

## Slide 48: Magnesium Minerals
Mineral | Formula | Class | Molar volume | Hard ness | Habit | Reference for Habit
Brucite | Mg(OH)2 | Brucite | 24.40 |  | Blocky pseudo hexagonal crystals. Platy or foliated masses and rosettes - fibrous to massive | http://webmineral.com/Alphabetical_Listing.shtml http://en.wikipedia.org/wiki/Brucite Notes 1, 2, 3
Brucite Hydrates | Mg(OH)2.nH2O | Brucite hydrates | ? | 2.5 | Not much known about them! | http://webmineral.com/Alphabetical_Listing.shtml
Pokrovskite | Mg2(CO3)(OH)2·0.5(H2O) | Basic | 66.79 | 3 | Brown radiating tufts. | http://mineralbliss.blogspot.com/2010/03/different-pokrovskite-habits-possible.html
Artinite | Mg2(CO3)(OH)2•3(H2O) | Basic | 105.81 | 2.5 | Bright, white acicular sprays Forms crusts of acicular crystals, elongated [010]. Also botryoidal masses of silky fibers; spherical aggregates of radiating fibers; cross-fiber veinlets. | http://webmineral.com/Alphabetical_Listing.shtml http://www.mindat.org/min-377.html
Hydromagnesite | Mg5(CO3)4(OH)2.4H2O | Basic | 221.86 | 3.5 | Include acicular, lathlike, platy and rosette forms Crystals small, occurring as tufts, rosettes, or crusts of acicular or bladed crystals elongated [001] and flattened {100}. Massive, chalky. | http://webmineral.com/Alphabetical_Listing.shtml http://www.mindat.org/show.php?id=1979&ld=1
Dypingite | Mg5(CO3)4(OH)2.5H2O | Basic | 181.45 | 181.45 | Numerous individual crystals or clusters. Globular - Spherical, or nearly so, rounded forms (e.g. wavellite). | http://webmineral.com/data/Dypingite.shtml

## Slide 49: Magnesium Minerals
Mineral | Formula | Class | Molar volume | Hard ness | Habit | Reference for Habit
Giorgiosite | Mg5(CO3)4(OH)2.5-6H2O | Basic | 183.93 | 3.5 | Fibrous and spherulitic, admixed with other species in powdery masses. | http://www.mindat.org/min-1979.html
Magnesite | MgCO3 | Normal or “self setting” | 28.11 | 3.9 | Usually massive Crystals usually rhombohedral {1011}, also {0112}; prismatic rare [0001] with {1120} and {0001}, or tabular {0001}. Scalenohedral rare. Massive, coarse- to fine-granular, very compact and porcelainous; earthy to rather chalky; lamellar; coarsely fibrous | http://webmineral.com/Alphabetical_Listing.shtml http://www.mindat.org/min-2482.html
Barringtonite | MgCO3·2H2O | Normal or “self setting” | 42.53 | 2.5 | Glassy blocky crystals | http://webmineral.com/Alphabetical_Listing.shtml
Nesquehonite | MgCO3·3H2O | Normal or “self setting” | 74.79 | 2.5 | Acicular prismatic needles Crystals prismatic, elongated along [010], {001}, {010}, {011}, {101}. {110} deeply striated parallel to [010]. Forms radial sprays and coatings, also botryoidal. | http://webmineral.com/Alphabetical_Listing.shtml http://www.mindat.org/min-2885.html
Lansfordite | MgCO3·5H2O | Normal or “self setting” | 102.59 | 2.5 | Glassy blocky crystals Minute short-prismatic crystals [001]; also stalactitic. | http://webmineral.com/Alphabetical_Listing.shtml http://www.mindat.org/min-2324.html

## Slide 50: Why Nesquehonite for Synthetic Carbonate Binder and Aggregate?
Nesquehonite has an ideal shape that contributes strength to the microstructure of a composite like concrete
Nesquehonite can be
  manufactured easily using the N-Mg sub-process at room temperature with little energy
  used directly in many products such as acoustic panels, non structural panels, insulation etc.
Nesquehonite is
  Stable over a wide PT range. It changes with heat to MgCO3 which is even more stable.
  A source input for the manufacture of reactive magnesia used in our cements
  Used to make our synthetic carbonate and waste aggregate
XRD Pattern Nesquehonite
Nesquehonite courtesy of Vincenzo Ferrini, university of Rome.
Mg++ + 3H2O + CO3-- => MgCO3·3H2O

## Slide 51: Structure of Nesquehonite
Stephan G W , MacGillavry C H , Acta Crystallographica, Section B , 28 (1972) p.1031-1033, The crystal structure of nesquehonite, MgCO3*3H2O
Infinite chains of MgO6 octahedra and CO3 groups hydrogen bonded together. Note that the atomic arrangement in nesquehonite shows no close relationship to those of the other known hydrated magnesium carbonates
Giester, G., Lengauer C. L. , and Rieck B. , The crystal structure of nesquehonite,
MgCO3.3H 2 O, from Lavrion, Greece, Mineralogy and Petrology (2000) 70: 153–163

## Slide 52: The Production of Nesquehonite
TecEco’s role
Conversion of a batch to continuous automated process. Tec-Kiln development
Source pictures : De Vito, Caterina, Ferrini,Vincenzo & Mignardi, Silvano, Ex situ CO2 mineralization via nesquehonite: a first attempt for an industrial application. Department of Science, Univeristy of Rome.
A batch process is working and has been built by colleagues at the University of Rome, La Sapienza

## Slide 53: Manufactured Aggregates – Using Synthetic Carbonates, Fly ash and other Wastes
Sand and stone aggregate are in short supply in some areas.
  Note that rMgO will neutralise salts and humus.
Nesquehonite is an ideal mineral for the manufacture of rMgO (our binder) as well as synthetic carbonate.
  rMgO => Mg(OH)2 => MgCO3.3H20 has high molar volume growth
  Ideal microstructure
  Stability
  Ideal low pH
  Polar bonds in composites making it suitable for binding wastes
Nesquehonite sequesters significant amounts of CO2

## Slide 54: Gaia Engineering Overview
Extraction Process
Fossil fuels
Solar or solar derived energy
Oil
rMgO
CO2
Coal
CO2
CO2
CO2
Inputs:
Atmospheric or industrial CO2, brines (e.g. de-sal and process waste water, other wastes
Outputs:
Carbonate building materials, HCl, fresher water.
Carbon or carbon compounds Magnesium compounds
1.29 gm/l Mg .412 gm/l Ca
Gaia Engineering is an industrial ecology that delivers profitable outcomes whilst reversing underlying undesirable moleconomic flows from other less sustainable carbon emitting processes.
Carbonate building components
Eco-Cement
TecEco Kiln
MgCO3.3H2O
TecEco N-Mg Process

## Slide 55: Gaia Engineering
MgCO3.3H2O
N-Mg Process
NH4Cl or HCl
Industrial CO2
rMgO
TecEco Tec-Kiln
Eco-Cements
Building components & aggregates
TecEco Cement Manufacture
CaO
Clays
Portland Cement Manufacture
Brine, Sea water, Oil Process water, De Sal Waste Water etc .
Tec-Cements
Other wastes
Fresh Water
GBFS
Fly ash

## Slide 56: Gaia Engineering

## Slide 57: Gaia Engineering Simplified

## Slide 58: The Potential of CO2 Release and Capture - Nesquehonite (MgCO3.3H2O) (N-Mg) Route
No Capture during Calcination
CO2
Carbon neutral except for process emissions
Use of non fossil fuels => Low or no process emissions
MgO
H2O
Mg(OH)2
H2O
Net Emissions 0.385 Kg CO2/Kg product
17 Source Data: http://www.tececo.com/files/spreadsheets/TecEcoCementLCA14Feb2011.xls
Net Energy 7435 kJ/kg product
<4500C
H2O
Capture during Manufacture MgCO3.3H2O
Net sequestration
H2O
Net Energy 100 kJ/kg product
CO2
Waste Mg++
Net Emissions (Sequestration) - 1.078 kg CO2/kg product
MgCO3.3H2O
MgCO3.3H2O

## Slide 59: The Potential of CO2 Release and Capture - Nesquehonite (MgCO3.3H2O) (N-Mg) Route
Capture during Calcination & Setting
Capture during Manufacture MgCO3.3H2O
CO2 from atmosphere
CO2 capture (e.g. N-Mg process etc.)
Net sequestration
Net sequestration less carbon from process emissions
Use of non fossil fuels => Low or no process emissions
MgO
Mg(OH)2
H2O
H2O
H2O
MgCO3.3H2O
Net Emissions (Sequestration) - .399kg CO2/kg product
17 Source Data: http://www.tececo.com/files/spreadsheets/TecEcoCementLCA14Feb2011.xls
H2O
Net Energy 7140 kJ/kg product
Net Energy 100 kJ/kg product
<4500C
Waste Mg++
MgCO3.3H2O
Net Emissions (Sequestration) - 1.078 kg CO2/kg product
CO2

## Slide 60: The N-Mg Process
The process is not dissimilar to the well know Solvay process
Tec-Kiln
NH3
MgCO3.3H2O
rMgO
CO2
NH4Cl
Filter
Filter
Mg rich water
MgCO3.3H2O
NH3
HCl

## Slide 61: Rapid Low Cost Production of Carbonate
Results with MgCl2 solution
Source pictures : Ferrini, V., De Vito, C. & Mignardi, S., 2009. Synthesis of nesquehonite by reaction of gaseous CO 2 with Mg chloride solution: Its potential role in the sequestration of carbon dioxide. Journal of Hazardous Materials, 168.

## Slide 62: Speciation of Carbonate pH dependent
MgCO3.3H2O precipitation

## Slide 63: Precipitation of Nesquehonite
The overall reactions are pH dependent and as follows:
1. CO2 + H2O < = > H2CO3 (aq)
2. H2CO3 (aq) < = > H+ (aq) + HCO3- - (aq)
3. Mg++(aq) + HCO3- - (aq) + 3H2O => MgCO3.3H2O (nesquehonite) + H+ (aq)
(results in acidification)
4. NH4OH + H+ (aq) => NH4+ (aq)+ H2O (results in neutralisation . Excess ammonia results in pH adjustment to produce a preponderance of HCO3- (aq) consumed in reaction 3. (See also the previous speciation graph. It is also possible that ammonia complexes assist the precipitation of nesquehonite (MgCO3.3H2O)).
5. NH4 + (aq) + Cl-- (aq) => NH4Cl (used industrially or used to make HCl by evaporating off ammonia)
Our preferred option is to use our Tec-Kiln to produce rMgO for our cements and a small amount to dissolve in water to produce Mg(OH)2
6. Mg(OH)2 + NH4Cl => MgCl2 + NH4OH (much less because most of the cycle Mg has been precipitated out as nesquehonite by the consumption of CO2. Both are recycled back in the process)

## Slide 64: Agglomeration of Synthetic Carbonates, Fly ash and other Wastes
Sand and stone aggregate are in short supply in some areas.
Nesquehonite is an ideal micro aggregate so why not agglomerate it and/or other magnesium carbonates to make synthetic (manufactured) aggregate?
MgO binders will be suitable for this purpose and TecEco are seeking funding to demonstrate the technology.
TecEco can already agglomerate fly ash and nesquehonite without additional energy. We just can’t tell you how as we have not had the money to pursue a patent.

## Slide 65: The TecEco Tec-Kiln
An obvious future requirement will be to make cements without releases so TecEco are developing a top secret kiln for low temperature calcination of alkali metal carbonates and the pyro processing and simultaneous grinding of other minerals such as clays.
The TecEco Tec-Kiln has no releases and is an essential part of TecEco's plan to sequester massive amounts of CO2 as man made carbonate in the built environment .
The TecEco Tec-Kiln has the following features:
Operates in a closed system and therefore does not release CO2 or other volatiles substances to the atmosphere.
  The CO2 produced will be recycled in the N-Mg process.
Can be powered by various potentially cheaper non fossil sources of energy such as intermittent solar or wind energy and is energy smart.
Grinds and calcines at the same time thereby running 25% to 30% more efficiently.
Produces more precisely definable product. (Secret as disclosure would give away the design)

## Slide 66: The Calcination of Nesquehonite (Tec-Kiln, N-Mg route)
Scope for Reducing Energy Using Waste Heat?
Initial weight loss below 100oC consists almost entirely of water (1.3 molecules per molecule of nesquehonite). Between 100 and 1500C volatilization of further water is associated with a small loss of carbon dioxide (~3-5 %).
From 1500C to 2500C, the residual water content varies between 0-6 and 0-2 molecules per molecule of MgC03. Above 3000C, loss of carbon dioxide becomes appreciable and is virtually complete by 4200C, leaving rMgO with a small residual water content.
Energy could be saved using a two stage calcination process using waste energy for the first stage.
1 mole of nesquehonite (solid) gives 3 moles of water (gas) and one off CO2 (gas). This is a significant molar volume expansion and could be used to drive a turbine or pistons to generate electricity.
Source: Dell, R. M. and S. W. Weller (1959). "The Thermal Decomposition of Nesquehonite MgCO3 3H20 And Magnesium Ammonium Carbonate MgCO3 (NH4)2CO3 4H2O." Trans Faraday Soc 55(10): 2203 - 2220.

## Slide 67: Gaia Engineering - An Example of Geomimetric Industrial Symbiosis!
N-Mg Process
TecEco Tec-Kiln
CO2
Nesquehonite
Nichromet Process
TecEco Cements
Direct Products
Reactive MgO

## Slide 68: Geomimicry
Carbonate sediments such as these cliffs represent billions of years of sequestration and cover 8% of the crust.
There are 1.2-3 grams of magnesium and about .4 grams of calcium in every litre of seawater.
There is enough calcium and magnesium in seawater with replenishment to last billions of years at current needs for sequestration.
To survive we must build our homes like these seashells using CO2 and alkali metal cations. This is geomimicry

## Slide 69: Gaia Engineering can Balance the Carbon Cycle
Photosynthesis by plants and algae
Consumed by heterotrophs (mainly animals)
Organic compounds made by autotrophs
Organic compounds made by heterotrophs
Cellular Respiration
Limestone coal, oil and gas burning
Gaia Engineering
Decay by fungi and bacteria
CO2 in the air and water
biomimicry

## Slide 70: Replacement of Portland Cement by Limestone
On the surface seems to be a good idea
Makes sense in relation to particle packing
Not however the best possible additive in terms of the chemistry
  pH is buffered down and pozzolanic and other important reactions including carbonation in our Eco-Cements is compromised.
“Limestone is generally considered to be the poorest potential performer of the available suite of mineral additions and as such considerable effort is focused on developing Portland-limestone cements that achieve the current general purpose Portland cement performance”1
We agree. Reactive magnesia (rMgO) or even ground SCM’s work much better as the resulting chemical reactions are beneficial. It may be that gypsum is not required with rMgO resolving a number of other issues.
I suggest the industry stop trying to be alchemists and go do a course in chemistry 101.
In the meantime please continue to make “Limestone Free Cement” for the benefit of down process blenders.
1Compton M, Chandler J., Elevated limestone mineral addition impacts on laboratory and field concrete performance. Concrete in Australia. 2012, 38(1):27 ‑ 33.

## Slide 71: Replacement of Cement by SCM’s
Portlandite should not be left in concretes because it is far too reactive.
Portlandite should be replaced by an alternative pH buffer
Portland cement can be blended with pozzolans such as fly ash which will consume Portlandite (Ca(OH)2) in the pozzolanic reaction.
It is important however that not all of the Portlandite is consumed as calcium will start leaching from CSH if it is.
As an alternative pH buffer we recommend the addition of rMgO which hydrates to Brucite. The equilibrium pH of Brucite is approximately 10.5 and the pH of CSH around 11.2 (22). The pH of a CSH and Brucite assemblage in equilibrium will not fall much below 10.5 and is ideal for immobilising heavy metal cations*.
* Important if we are to use wastes like fly ash.

## Slide 72: Mix Optimisation
Mix optimisation is mostly an art and should be a science. It is not practiced widely enough and there are a lot of shortcuts in the software used.
A pioneer in this field is Francois de Larrard from France.
The next area to consider in in mix design software is volume stoichiometry and particle charge affects.
Particle charge is very important in relation to the rapid setting and strength gain in high SCM Tec-Cement mixes.

## Slide 73: Product Differentiation and Specialisation
New mineral composites incorporating waste streams that add properties sought such as thermal flow resistance, fire resistances etc. are required.
  Important in relation to reducing the lifetime energies of structures
  Important in relation to adding value to waste streams facilitating their conversion to resources and reducing pollution
To allow this to be achieved prescription based standards need to be scrapped and relegated to the role of practice guides.
Broadly based performance criteria are essential.

## Slide 74: Changing the Emphasis
In relation the sustainability more emphasis should be placed on aggregates as they comprise 80% of concrete.
A greater emphasis on properties not prescriptions.
A wider emphasis on the range of cementitious composites.
  Addressing lifetime energy, sound insulation and a wide range of other requirements other than just strength and thermal mass.

## Slide 75: The Right Business Models
Cost cutting business models will not get the industry to where it needs to go
Innovation based business models and appropriate changes to standards are required.
Increases in Business Performance by Innovation status 2008 – 9

## Slide 76: Cost rather than Profit Based Business Models
Most corporations in the concrete industry have business model that relies on significant turnover and cost cutting to deliver profit.
  Research and development budgets that deliver innovations and potentially more profitable product are generally small.
  A focus on cost instead of cost effective.
If the industry believe in “cutting edge” research then they are going to have to practice what they preach and support innovation.
In Australia there is now benchmark support for R & D and commercialisation

## Slide 77: Examples of Other Huge Change Opportunities
A wide variety of possible end uses with higher potential margins for which current solutions are sub-optimal.
  E.g. Addressing properties affecting lifetime energy.
    E.g. Mineral composites with higher “R” value viz.
    Boards made with mineral binders & wastes - “MgO boards”
    Exterior structural panels with insulating properties
Huge opportunities for reducing the cost base and improving the properties of concretes by focusing on the process by which they are made and what they are made with.
  A few tweaks to the formulations
  Major changes to the process and some
  Lateral thinking in relation to aggregates => Synthetic carbonate aggregate.
De-materialization through design (Reductions in Kg CO2-e/Mpa)7
Improvements in durability. Missing from the current analyses for sustainability
See Part 2 for the ramifications of using reactive MgO
7 Wallenvik, Olafur, Carbon Footprint of High Performance Versus Conventional Vibrated Concrete

## Slide 78: Innovation – Turning Buildings the Right Way Out
Mineral composites with high “R” value can easily be made using reactive magnesia because of the polar bonding capacity (See Part 2). Hydration and carbonation products of reactive magnesia are all fire retardants. Imagine the reduction in lifetime energies if we started constructing buildings the right way out!
Mineral composites with low conductance ~ high “R” value and fire resistance
Mineral composites with high thermal capacity
Conventional timber framing and plaster
Mineral composites with high thermal capacity

## Slide 79: Barriers to Innovation and Change
Out of date and inappropriate legislative restriction.
  See other presentations
A prescription rather than performance based standards and approvals system. and other presentations as well as what I have to say.
A corrupt patent System.
  Governments tend to issue patents to anyone for the money
  A lack of know how in patent offices as a result of low pay
Lack of transparency in relation to new products.
  Secret formulations more often than not in breach of other people’s ip.
Knowledge should be free
  Wikipedia v Science Direct etc.
Greenwash.
A focus on cost instead of cost effective
  Little or no support for “cutting edge research” (See Lionel Lemay’s presentation4)
Conservatism (Goes without saying?)
A low level of skills in the industry
Conflicting
9 Lobo, Colin, The role of Performance Based Specification in Sustainable Development
10 Mansour, Wassim, Towards Performance-based Specification – Case Studies on Construction Projects in Abu Dhabi 11 Lemay, Lionel, Life cycle Assessment of Concrete Structures

## Slide 80: The Right Framework to Operate In - Standards
The concrete industry in most countries operates with a restrictive framework of standards and guides and supporting legislation that breeds
  conservative managers who do not innovate
  cost cutting business model.
Change must occur if we are to move forward on sustainability and take advantage of emerging opportunities for carbon trading.
  Given the lack of training and education at the base level this will be a difficult challenge.
Performance based standards are essential. Existing standards should be converted to guides.

## Slide 81: The Standards and Approvals Systems
Far too often our standards and approvals ratings are prescription based stifling innovation and change.
Even Leeds in the US and the Green Building Council in Australia make the same mistake
Standards should be based on a list of metrics for properties including embodied energy and emissions, thermal capacity and conductance, strength (compressive, shear and flexural) etc.
This means that many existing standards should be relegated to being “codes of practice”
Proper audit process instead??
  See Colin Lobo’s presentation (NRMCA)

## Slide 82: The Right Framework to Operate In – Legislative Framework
Too much restriction stifles innovation.
A better approach would be better training in the industry.
Few governments have ever managed to get the mix of stick, incentive and procurement right or even remotely efficient.
Governments do not follow their policies through the supply chain.
  Procurement policies must follow R & D support.
UKIERI and other bodies need to take a greater leadership role.

## Slide 83: Conservatism
With the exception of perhaps the architectural fraternity players in the construction industry are generally conservative
There is little incentive and a lot of risk in using new materials that have reduced embodied energies and emissions and substantial impact on reducing lifetime energies.
One of the reasons for this conservatism is the legal liability of designers and engineers.
Perhaps prescription standards should become codes of practice and greater support given for testing of new materials.
Audited procedures and less reliance on standards?

## Slide 84: The Low Level of Skills in the Industry
There is an appallingly low level of skills in the concrete industry.
  Electricians and plumbers must have licenses in most countries yet concrete placers and finishers seldom have any training at all.
  Most civil engineers are taught very little and understand less about the material they use every day.
It is no wonder we have the attitude that all that is grey is great, all we make goes out the gate. (With affront meant to Grey Matters)
  any diversion is risky!
This terrible situation needs to change.
  Congratulations to the NRMCA re their producer training programs but what about placers and finishers?
Quality control should go beyond testing, it must include risk management through training.

## Slide 85: A Corrupt Global Patent System
Patents are taken far to literally; the intent and purpose are almost irrelevant.
Most patent examiners are basically incompetent – How could they be otherwise?
The revenue raised is of greater importance to the grantee government than the value of the so called monopoly rights given.
Patents are an invitation and challenge to others to steal ip.
  Many secret formulations end up being identified as stolen ip.
Governments do not protect the ip they “grant” they let the players fight it out in court.
It follows that patents are little more than meat for dogs to fight over.
  Consider geopolymers for example and my own experience.

## Slide 86: The Role of Reactive MgO – An Update on TecEco Technology
An update on recent advances in Tec and Eco-Cements including the use of high proportions of fly ash and SCMS with added reactive magnesia
Reactive Magnesia is the most powerful new tool in cement chemistry

## Slide 87: TecEco Cements
Eco-Cements have relatively high proportions of magnesia which in permeable materials carbonates adding strength and durability. Eco-Cement formulations are generally used for bricks, blocks, pavers, pervious pavements and other permeable cement based products. See http://www.tececo.com/products.eco-cement.php
Enviro-Cements are made using large quantities of reactive magnesia which reacts to form Brucite. Brucite is unique to TecEco Cements and is an ideal mineral for trapping toxic and hazardous wastes due to its layered structure, equilibrium pH level, durability and low solubility. See http://www.tececo.com/products.enviro-cement.php
Tec-Cements are cement blends that comprise of a hydraulic cement such as Portland cement mixed with a relatively small proportion of reactive magnesia and optionally pozzolans and/or supplementary cementitious materials which react with Portlandite removing it and making more cement or are activated by Portland cement. They offer a solution to many of the technical problems that plague traditional cement formulations caused by the reactivity of lime (Portlandite) and have significant advantages including faster setting even with a high proportion of non PC additions. See http://www.tececo.com/products.tec-cement.php

## Slide 88: TecEco Eco-Cements
Left: Recent Eco-Cement blocks made, transported and erected in a week. Laying and Eco-Cement floor. Eco-Cement mortar & Eco-cement mud bricks. Right: Eco-Cement permeacocretes and foamed concretes
Eco-Cements are blends of one or more hydraulic cements and relatively high proportions of reactive magnesia with or without pozzolans and supplementary cementitious additions. They will only carbonate in gas permeable substrates forming strong fibrous minerals such as lansfordite and nesquehonite. Water vapour and CO2 must be available for carbonation to ensue.
Eco-Cements can be used in a wide range of products from foamed concretes to bricks, blocks and pavers, mortars renders, grouts and pervious concretes such as our own permeacocrete. Somewhere in the vicinity of the Pareto proportion (80%) of conventional concretes could be replaced by Eco-Cement.
Light colour = low albedo

## Slide 89: Forced Carbonation ~ Optimisation
 | Forced Carbonation (Cambridge) | Kinetic Optimisation (TecEco)
Steps | Multistep process | Less steps = lower costs
Rate | Variable | Varying on weather conditions (wet dry best and gas permeability)
% Carbonation in 6 months | 70% (reported, could be more if permeable) | 100%
Ease of general implementation | Require point sources CO2 | Can be implemented very quickly
Can use large quantities of fine wastes | Can use large quantities of fine wastes like fly ash that are not necessarily pozzolanic | Fine wastes tend to reduce gas permeability
Safety | Are carbonation rooms safe? | No issues
Key requirements | Special carbonation rooms | Optimal kinetics including gas permeability
Physical rate considerations | Doubling the concentration of CO2 doubles the rate of carbonation. | Doubling the pore size quadruples the rate of carbonation.
Other issues | Able to be sealed with paint etc. as pre carbonated | Some sealing paints will slow down carbonation
Forced carbonation of silicate phases as promoted by some is nonsense
20 According to ECN "The CO2 concentration in power station flue gas ranges from about 4% (by volume)for natural gas fired combined cycle plants to about 14% for pulverised coal fired boilers." At 10% the rate increase over atmospheric could be expected to be 10/.038 = 263 times provided other kinetic barriers such as the delivery of water do not set in. Ref: http://www.ecn.nl/en/h2sf/products-services/co2-capture/r-d-activities/post-combustion-co2-capture/ accessed 24 Mar 08.

## Slide 90: Carbonation Optimisation
Dissolution of MgO
  Gouging salts e.g. MgSO4, MgCl2 and NaCl (Not used by TecEco)
  Various catalysing cations e.g. Ca ++ and Pb ++ and ligands EDTA, acetate, oxalate citrate etc. (Not used by TecEco)
  Low temperature calcination = Low lattice energy = high proportion of unsaturated co-ordination sites = rapid dissolution. See http://www.tececo.com/technical.reactive_magnesia.php
Carbonation – High concentration of CO3-- at high pH as a result of OH- from Portlandite
Possible catalysis and nucleation by polar surface of calcium silicate hydrate at high pH
Wet dry conditions. Wet for through solution carbonation, dry for gas transport.
Gas permeability
Carbonate shape is important (next slides)

## Slide 91: Particle Packing – Percolation and Porosity ~ Permeability
Shape effects particle packing (Olafur Wallevik presentation21 ) and the angle of repose (Bagnold22). The latter is therefore a proxy guide to shape.
Eco-Cements are deliberately not perfectly packed. Whereas in Tec-Cements the opposite occurs
21Wallenvik, Olafur, Carbon Footprint of High Performance Versus Conventional Vibrated Concrete
22Bagnold, Ralph A, The Physics of Blown Sand and Desert Dunes

## Slide 92: Economics of Magnesium Carbonate Binder Based Masonry Products
What this embedded spreadsheet demonstrates is that Magnesium Carbonate Block formulations are uneconomic unless the price of reactive MgO approaches that of PC or there is a high price for carbon or alternatively less MgO can be used!
Because of molar volume growth less can be used but we must still address supply chain issues.
This embedded spreadsheet looks only at the binder price and assumes all other factors remain the same

## Slide 93: Permeacocretes
Permeacocretes are an example of a product where the other advantages of using reactive MgO overcome its high cost.
The use of MgO gives an ideal rheology which makes it possible to make permeacocrete pervious pavements using conventional road laying equipment therefore substantially reducing labour costs.
There are many other advantages of pervious pavements see http://www.tececo.com/files/conference%20presentations/TecEcoPresentationSGA25Mar2010.ppt
We are developing a low cost method of mechanised placement.

## Slide 94: Tec-Cements
Tec-Cements (5-20% MgO, 80-95% OPC)
  contain more Portland cement than reactive magnesia. Reactive magnesia hydrates in the same rate order as Portland cement forming Brucite which uses up excess water reducing the voids:paste ratio, increasing density and possibly raising the short term pH.
  Reactions with pozzolans are more affective. After much of the Portlandite has been consumed Brucite tends to control the long term pH which is lower and due to it’s low solubility, mobility and reactivity results in greater durability.
  Other benefits include improvements in density, strength and rheology, reduced permeability and shrinkage and the use of a wider range of aggregates many of which are potentially wastes without reaction problems.

## Slide 95: Water – Fundamental to Concretes
Polar Bonding
Diagrammatic representation of a water molecule having polar covalent bonds between the Oxygen atom and the Hydrogen atoms. (Note the angle is supposed to be 104.5 oC)
In a polar covalent bond, the electrons shared by the atoms spend a greater amount of time, on average, closer to the oxygen nucleus than the hydrogen nucleus. This is because of the geometry of the molecule and the great electronegativity difference between the hydrogen atom and the oxygen atom.
The result of this pattern of unequal electron association is a charge separation in the molecule, where one part of the molecule, the oxygen end, has a partial negative charge and the hydrogens have a partial positive charge.

## Slide 96: The Electrostatic Nature of Cements made with Water
The surface tension of water is 73 dynes per cm at 18oC compared to ethyl alcohol at 24 dynes per cm.
Hydrogen bonding is attributed to the ability of water to adhere to or “wet” most surfaces; such substances are said to be hydrophilic (water-loving). A hydrogen bond is only about 10 percent of the strength of a covalent bond, but it is responsible for most of the unusual properties of water (high freezing and boiling points, high heat capacity, high heats of fusion and evaporation, solvency, and high surface tension).
Water has an exceptionally large dipole moment (1.87 x 10-18 e.s.u.) relative to most other inorganic compounds. Dipole moment is the product of the distance
between the charges multiplied by the magnitude of the charge in electrostatic units (e.s.u.).
23Refer: Labbe, Christophe, Nonat, Andre, 2007, The Cement Cohesion: An Affair of Electrostatics, Lutam Symposium on Swelling and Shrinkage of Porous Materials, Petropolis, Brazil

## Slide 97: Wet Stage Properties of Tec-Cement Concretes
Water has cohesivity due to a network of extensive three-dimensional hydrogen bonding and this property is strengthened both by Brucite surfaces and the strongly kosmotropic Mg++ ion.
The strong polar bonding
  Affects all wet stage properties
    Improved rheology markedly (all formulations)
    Dissolution of SCM’s like clinker, gbfs etc.
    High early strength
    Greater strength
    Reduced bleed water thereby retaining alkali
    Reduced early age shrinkage
  Significantly brings forward the onset of first set with high replacement mixes.
    Increases the “wet sand effect” effect.
    MgO goes negative
  Reduces overall shrinkage incl. autogenous shrinkage
Ca++ = 114 picometres Mg++ = 86 picometres

## Slide 98: The Effect of a Strong Kosmotrope such as Mg++
++
The polar bonding of water is supercharged by the presence of a strong cation such as Mg++ which has a strong affinity for the oxygen end of water.
The supercharging of the polar bonding of water and other hydrated species will propagate and may cause more rapid dissolution of clinker, GBFS and other hydraulic cements leading to earlier more complete reaction and thus early strength.
++
-
Supposed to be 104.5 deg.

## Slide 99: Dissolution – By Proton Wrenching?
According to Pellenq from MIT water dissociates and the protons formed move in a Grotthus like way (i.e. by proton hopping) penetrating the crystal structure of alite and play a role in breaking it apart. Belite has a different crystal structure and this does not occur to the same extent. Pellenq suggests change Belite structure using aluminium. We mention that aluminium works in our patents at length so have the prior art however Pellenq et. al. add understanding as to possibly why. We suggest changing the nature of water by adding Mg++. (See later, note both methods work well together)
Magnesium is mainly present as Mg2+ (aq) in water, but also as MgOH+ (aq) and Mg(OH)2 (aq) and other species. The strong electron pull of magnesium may also play a role in dissolution as we have noticed a much faster early setting rate and can make cements with pure gbfs for example. i.e Mg++ and associated aqueous species probably play a role in dissolution processes.
24 Image Source: Slide in a presentation by Prof Roland Pellenq, MIT Concrete Sustainability Hub
Dissolution of alite by proton wrenching

## Slide 100: Setting – An Electrostatic Affair?
The Wet Beach affect
Sand is largely silica that has broken into small grains. At the atomic scale, silica
consists of a three-dimensional network of covalently bonded silicon and oxygen atoms.
Typically, silica surfaces contain mostly oxygen atoms, many of which are covalently bonded to hydrogen atoms.
The surface contains many polar bonds and can hydrogen-bond to water molecules. Therefore water is attracted to silica
surfaces, which are said to be hydrophilic (water loving).

## Slide 101: MgO has a Bar Magnet Effect
The Change in the Surface Charge of Metal Oxides with pH.
25Source:Small, R.J. et al., 2005. Using a buffered rinse solution to minimize metal contamination after wafer cleaning. MicroMagazine.com. Available at: http://www.micromagazine.com/archive/98/01/small.html.

## Slide 102: High and Total Replacement Cements
TecEco recently announced a way forward to greater sustainability for the Portland cement industry.
Up to 30% or more strength at all stages with high & very high replacement ternary mixes. (GBFS +- fly ash replacing PC.)
Total replacement with class C fly ash and gbfs is possible
Finishers can go home early using >50% replacement mixes removing the remaining barrier to their implementation.
Brilliant rheology, low shrinkage and little or no cracking.
Excellent durability.
A solution to autogenous shrinkage?
Mixes with MgO can tolerate carbon in fly ash and clays to some extent.
Mg++ combines with chloride or sulfate immobilising these cations
Mg++ neutralises humus in sands
Mg(OH)2 provides long term pH control protecting steel.

## Slide 103: Example Results for TecEco
Date of Trial Mix | 30/10/2010 20MPa |  | 3/12/2010 32MPa | 
Constituents | Kg | % | Kg | %
GP PC, kg/m3 | 116 | 47.93 | 155 | 47.78
Fly ash, kg/m3 | 58 | 23.97 | 78 | 24.04
Slag, kg/m3 | 58 | 23.97 | 78 | 24.04
Reactive Magnesia, kg/m3 | 10 | 4.13 | 13.4 | 4.13
MgO relative to PC |  | 8.7 |  | 8.7
20mm, kg/m3 | 710 |  | 730 | 
10mm, kg/m3 | 275 |  | 280 | 
Total Coarse Aggregate | 985 |  | 1010 | 
Manufactured Sand, kg/m3 | 490 |  | 440 | 
Fine Sand, kg/m3 | 390 |  | 350 | 
Total Fine Aggregate | 880 |  | 790 | 
WR (WRDA PN), ml/100kg | 350 |  | 400 | 
Water, lt/m3 | 185 |  | 199 | 
Design Slump, mm | 80 |  | 100 | 
Actual Slump, mm | 80 |  | 100 | 
Strength | 20 Mpa |  | 32MPa | 
3 Day | 13.0 |  | 17.0 | 
7 Day | 18.0 |  | 24.5 | 
28 Day | 32.5 |  | 42.5 | 
56 Day | 39.0 |  | 46.5 | 
Shrinkage | 20 Mpa |  | 32MPa | 
1 week | 330 |  | 320 | 
2 week | 430 |  | 420 | 
3 week | 500 |  | 490 | 
4 week | 560 |  | 520 | 
7 week | 660 |  | 580 | 
Chart: 
| 3 Day | 7 Day | 28 Day | 56 Day
20 Mpa | 13 | 18 | 32.5 | 39
32MPa | 17 | 24.5 | 42.5 | 46.5
Chart: 
| 1 week | 2 week | 3 week | 4 week | 5 week | 6 week | 7 week
20 Mpa | 330 | 430 | 500 | 560 | 600 | 650 | 660
32MPa | 320 | 420 | 490 | 520 | 580
NB. Our patents in all countries define the minimum added % MgO as being >5% of hydraulic cement components or hydraulic cement components + MgO
Strength
Shrinkage

## Slide 104: A Tec-Cement Modified Ternary Mix

## Slide 105: Easier to Finish Concretes
Easier to pump and finish Concretes are likely to have less water added to them resulting in less cracking

## Slide 106: Brilliant Rheology
The strongly positively charged small Mg++ atoms attract water (which is polar) in deep layers introduce a shear thinning property affecting the rheological properties and making concretes less “sticky” with added pozzolan
It is not known how deep these layers get
Etc.
Etc.
Ca++ = 114, Mg++ = 86 picometres

## Slide 107: Bingham Plastic Rheology
TecEco concretes and mortars are:
  Very homogenous and do not segregate easily. They exhibit good adhesion and have a shear thinning property.
  Exhibit Bingham plastic qualities and react well to energy input.
  Have good workability.
TecEco concretes with the same water/binder ratio have a lower slump but greater plasticity and workability.
TecEco tec-cements are potentially suitable for mortars, renders, patch cements, colour coatings, pumpable and self compacting concretes.
A range of pumpable composites with Bingham plastic properties will be required in the future as buildings will be “printed.”

## Slide 108: Tec-Cement Mixes
 | Ordinary Mixes | TecEco Tec-Cement Mixes | Notes
Reactive MgO as defined | None | Usually 8 to 10% / PC added | 1
Pozzolan (Pos) | Should be used | Recommended. | 
Supplementary cementitious materials (SCM’s) | Should be used | Recommended. | 2
Limit on additions pozzolans + SCM’s | Limited by standards that are increasingly exceeded | > 50% recommended especially if a ternary blend | 
Rheology | Usually sticky, especially with fly ash. Hard to finish. | Slippery and creamy. Easy to finish. | 
Setting time | Slow. Especially with fly ash only. | Much faster. Blends with a high proportion Pos. and SCM’s set like ordinary PC concrete. | 
Shrinkage and cracking | Significant | Much less | 
Additives | Usually used | Not necessary | 
Durability | Without additions of SCM’s questionable. | Excellent especially with additions of SCM’s | 
28 day Strength (prev. 20 MPA mix) | < .20 Mpa/Kg PC/m3 | > .27 Mpa/Kg PC/m3 | 
$ Cost Binder/Mpa at 28 days (prev 20 & 32 MPa mixes) | > ($2.30-$2.50) | < ($1.50-$1.90) | 3
Notes 1. See http://www.tececo.com/technical.reactive_magnesia.php. % is relative to PC and in addition to amount already in PC
2. To keep our patents simple we included supplementary cementitious materials as pozzolans in our specification
3. See economics pages following
We recommend using both Pos and SCM’s together

## Slide 109: Why Put Brucite in Concretes?
Improved rheology (see http://www.tececo.com/technical.rheological_shrinkage.php)
Prevents shrinkage and cracking (see http://www.tececo.com/technical.rheological_shrinkage.php)
Provides low shrinkage and pH and eH control. Reduced corrosion. Stabilises CSH when Ca++ consumed by the pozzolanic reaction (Encouraged)
Relinquishes polar bound water for more complete hydration of PC thereby preventing autogenous shrinkage?
Solves the carbon in fly ash, sulfate, chloride and clay in aggregate problems.
Pourbaix diagram steel reinforcing
Equilibrium pH Brucite

## Slide 110: Immobilisation as Well as Encapsulation

## Slide 111: Dry Stage Properties of Tec-Cement Concretes
Significantly increased tensile strength
Increased compressive strength (especially early strength) particularly with high replacement mixes containing significant amounts of GBFS compacting factor
Reduced shrinkage and cracking
Improved durability
Higher tensile strain capacity?
Greater creep
Less permeable?
Lighter albedo
Solves autogenous shrinkage problems
May solve other delayed reaction problems
26Recommended Reading: Du C. A Review of Magnesium Oxide in Concrete - A serendipitous discovery leads to new concrete for dam construction. Concrete International. 2005;(December 2005):45 - 50.

## Slide 112: TecEco Tec-Cements – Eliminating Problems in Concrete
There are two fundamental factors affecting durability: transport and reactivity of reactants
Bad work is costly, looks lousy and usually compromises long term durability.
With TecEco Technology Much More Durable Concretes are Possible. Shrinkage, Delayed Reactions and Corrosion can be Substantially Eliminated

## Slide 113: A Crack Collage
TecEco technology can reduce if not solve problems of cracking:
  Related to (shrinkage) through open system loss of water.
  As a result of volume change caused by delayed reactions
  As a result of corrosion.
  Related to autogenous shrinkage
Thermal
Plastic Shrinkage
Drying Shrinkage
Corrosion Related
Freeze Thaw D Cracks
Structural
Settlement Shrinkage
Photos from PCA and US Dept. Ag Websites
Autogenous or self-desiccation shrinkage (usually related to stoichiometric or chemical shrinkage)
Alkali aggregate Reaction
Evaporative Crazing Shrinkage

## Slide 114: What Influences Durability?
Concretes are said to be less durable when they are physically or chemically compromised.
Physical factors can result in chemical reactions reducing durability
  E.g. Cracking due to shrinkage can allow reactive gases and liquids to enter the concrete
Chemical factors can result in physical outcomes reducing durability
  E.g. Alkali silica reaction opening up cracks allowing other agents such as sulfate and chloride in seawater to enter.

## Slide 115: Durability (Important for Sustainability)
Durability is related to physical and chemical factors
  How easy is it for an aggressive agent to get into the concrete matrix
    This depends on the density which depends on the voids and specific gravity of the minerals present.
      The number and size of voids depends on the particle packing and water added.
      If the number and size of voids causes percolation points to be exceeded then the material is permeable and thus not likely to be durable depending on the Eh-pH and chemical reactivity of species present.
      Strength is not the cause of strength but a bad proxy for permeability.
  What the aggressive agent can do once in there
    Depends on the Eh-pH conditions inside the matrix and presence or otherwise of Portlandite
      Ideally reducing Eh and pH above about 9.5 depending on the Eh.
      Brucite the hydration product of reactive MgO stabilises the pH in concrete. The equilibrium pH of Brucite is around 10.42.
      Reactive MgO will also remove chloride and sulfate by reacting with them.
      Consumes chloride and sulfate in the wet stage rendering them immobile.
  Protection of steel (pH control) and the electro coupling present
    e.g. steel – chloride
  Carbonation of Brucite is expansive and seals the surface.

## Slide 116: Causes of Cracking in Concrete
Cracking commonly occurs when the induced stress exceeds the maximum tensile stress capacity of concrete and can be caused by many factors including restraint, extrinsic loads, lack of support, poor design, volume changes over time, temperature dependent volume change, corrosion, carbonation or delayed reactions.
Causes of induced stresses include:
  Restrained thermal, plastic, drying and stoichiometric shrinkage, corrosion, carbonation and delayed reaction strains.
  Slab curling.
  Loading on concrete structures.
Cracking is undesirable for many reasons
  Visible cracking is unsightly
  Cracking compromises durability because it allows entry of gases and ions that react with Portlandite.
  Cracking can compromise structural integrity, particularly if it accelerates corrosion.

## Slide 117: Graphic Illustration of Cracking
After Tony Thomas (Boral Ltd.) (Thomas 2005)
Autogenous shrinkage has been used to refer to hydration shrinkage and is thus stoichiometric

## Slide 118: Cracking due to Loss of Water
Drying Shrinkage
Plastic Shrinkage
Picture from: http://www.pavement.com/techserv/ACI-GlobalWarming.PDF
Evaporative Crazing Shrinkage
Settlement Shrinkage
We may not be able to prevent too much water being added to concrete by fools. TecEco approach the problem in a different way by providing for the internal removal/storage of water that can provide for more complete hydration of PC.
Brucite gains weight in excess of the theoretical increase due to MgO conversion to Mg(OH)2 in samples cured at 98% RH.
Dr. Luc Vandepierre, Cambridge University, 20 September, 2005.
Bucket of Water
Fool

## Slide 119: Solving Cracking due Shrinkage from Loss of Water
In the system water plus Portland cement powder plus aggregates shrinkage is in the order of .05 – 1.5 %.
There are two root causes of Portland cements shrinking over time.
  Stoichiometric (chemical) shrinkage and
  Shrinkage through loss of water.
The solution is to:
  Add minerals that compensate by stoichiometrically expanding and/or to
  Use less water, internally hold water or prevent water loss.
  Prevent water exiting the system
TecEco tec-cements internally hold water and prevent water loss.
MgO (s) + H2O (l) ↔ Mg(OH)2.nH2O (s)

## Slide 120: Preventing Shrinkage through Loss of Water
When magnesia hydrates it consumes 18 litres of water per mole of magnesia probably more depending on the value of n in the reaction below:
MgO (s) + H2O (l) ↔ Mg(OH)2.nH2O (s)
The dimensional change in the system MgO + PC depends on:
  The ratio of MgO to PC
  Whether water required for hydration of PC and MgO is coming from stoichiometric mix water (i.e. the amount calculated as required), excess water (bleed or evaporative) or from outside the system.
  In practice tec-cement systems are more closed and thus dimensional change is more a function of the ratio of MgO to PC
As a result of preventing the loss of water by closing the system together with expansive stoichiometry of MgO reactions (see below).
MgO (s) + H2O (l) ↔ Mg(OH)2.nH2O (s)
40.31 + 18.0 ↔ 58.3 molar mass (at least!)
11.2 + liquid ↔ 24.3 molar volumes (at least!)
It is possible to significantly reduce if not prevent (drying, plastic, evaporative and some settlement) shrinkage as a result of water losses from the system.
  The molar volume (L.mol-1)is equal to the molar mass (g.mol-1) divided by the density (g.L-1).

## Slide 121: Preventing Shrinkage through Loss of Water
Portland cements stoichiometrically require around 23 -27% water for hydration yet we add approximately 45 to 60% at cement batching plants to fluidise the mix sufficiently for placement.
If it were not for the enormous consumption of water by tri calcium aluminate as it hydrates forming ettringite in the presence of gypsum, concrete would remain as a weak mush and probably never set.
  26 moles of water are consumed per mole of tri calcium aluminate to from a mole of solid ettringite. When the ettringite later reacts with remaining tri calcium aluminate to form monosulfoaluminate hydrate a further 4 moles of water are consumed.
The addition of reactive MgO achieves water removal internally in a closed system in a similar way.
MgO (s) + H2O (l) ↔ Mg(OH)2.nH2O (s)

## Slide 122: Other Benefits of Preventing Shrinkage through Loss of Water
Internal water consumption also results in:
  Greater strength
    More complete hydration of PC .
    Reduced in situ voids:paste ratio
  Greater density
    Increased durability
    Higher short term alkalinity
    More effective pozzolanic reactions.
More complete hydration of PC .
  Small substitutions of PC by MgO result in water being trapped inside concrete as Brucite and Brucite hydrates which can later self desiccate delivering water to hydration reactions of calcium silicates (Preventing so called “autogenous” shrinkage).

## Slide 123: Bleeding is a Bad Thing
Bleeding is caused by:
  Lack of fines
  Too much water
Bleeding can be fixed by:
  Reducing water or adding fines
  Air entrainment or grading adjustments
Bleeding causes:
  Reduced pumpability
  Loss of cement near the surface of concretes
  Delays in finishing
  Poor bond between layers of concrete
  Interconnected pore structures that allow aggressive agents to enter later
  Slump and plastic cracking due to loss of volume from the system
  Loss of alkali that should remain in the system for better pozzolanic reactions
  Loss of pollutants such as heavy metals if wastes are being incorporated.
Concrete is better as a closed system
Better to keep concretes as closed systems

## Slide 124: Open/Closed Systems - The Wet Sand Analogy
In the particulate state wet beach sand is held together by the surface tension of water (a ramification of hydrogen bonding)
A beach sand system emulates a closed system because water lost through evaporation or bleeding is constantly replaced by waves.
No plastic or drying shrink cracking is observable in wet beach sands.
To prevent plastic and drying shrink cracking in concrete the system must also be closed preventing loss of water through evaporation. To do this surface coatings such as aliphatic alcohols are used.
The TecEco method is to internally hold water in Brucite and its hydrates that would otherwise bleed or evaporate.
Increased surface tension in Tec-Cements reduces movement of water through capillaries and reduces evaporative loss
Concrete can be made totally shrink proof (foolproof)
  Adding reactive magnesia to consume and store water as it hydrates.
  Applying surface coatings e.g. aliphatic alcohol (e.g. ethylene glycol).
As a result joints are usually only necessary for structural reasons.
Wet sand or wet concrete? Wet concrete still in the particulate stage has much in common with wet sand

## Slide 125: Dimensionally Control Over Concretes During Curing?
Portland cement concretes shrink around .05%. Over the long term much more (>.1%).
  Mainly due to plastic and drying shrinkage through loss of water
The use of some wastes as aggregates also cause shrinkage e.g. wood waste in masonry units, thin panels etc.
By adding MgO volume changes are minimised
  So far we have observed significantly less shrinkage in TecEco tec - cement concretes with about (8-10% substitution OPC) with or without fly ash.
Note that Brucite is > 44.65 mass% water and it makes sense to make binders out of water!

## Slide 126: Greater Tensile Strength also Reduces Cracking
MgO Changes Surface Charge as the Ph. Rises. This and a stronger “wet beach effect” could be the reason for the greater tensile strength displayed during the early plastic phase of tec-cement concretes.
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Mutual Repulsion
=>
+
+
+
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
Ph. 12 ?
Cement
Cement
MgO
Sand
Sand
MgO
Mutual Repulsion
Mutual Attraction

## Slide 127: Reducing Cracking as a Result of Volume Change caused by Delayed Reactions
Photo Courtesy Ahmad Shayan ARRB
An Alkali Aggregate Reaction Cracked Bridge Element

## Slide 128: Types of Delayed Reactions
There are several types of delayed reactions that cause volume changes (generally expansion) and cracking.
  Alkali silica reactions
  Alkali carbonate reactions
  Delayed ettringite formation
  Delayed thaumasite formation
  Delayed hydration or dead burned lime or periclase.
Delayed reactions cause dimensional distress, cracking and possibly even failure.

## Slide 129: Reducing Delayed Reactions
Delayed reactions do not appear to occur to the same extent in TecEco cements.
  A lower long term pH results in reduced reactivity after the plastic stage.
  Potentially reactive ions are trapped in the structure of Brucite.
  Ordinary Portland cement concretes can take years to dry out however the reactive magnesia in Tec-cement concretes consumes unbound water from the pores inside concrete.
  Magnesia dries concrete out from the inside. Reactions do not occur without water.

## Slide 130: Reduced Corrosion Related Cracking
Steel remains protected with a passive oxide coating of Fe3O4 above pH 8.9.
A pH of over 8.9 is maintained by the equilibrium Mg(OH)2 ↔ Mg++ + 2OH- for much longer than the pH maintained by Ca(OH)2 because:
  Brucite does not react as readily as Portlandite resulting in reduced carbonation rates and reactions with salts.
Concrete with Brucite in it is denser and carbonation is expansive, sealing the surface preventing further access by moisture, CO2 and salt.
Rusting Causes Dimensional Distress

## Slide 131: Reduced Corrosion Related Cracking
Brucite is less soluble and traps salts as it forms resulting in less ionic transport to complete a circuit for electrolysis and less corrosion.
Free chlorides and sulfates originally in cement and aggregates are bound by magnesium
  Magnesium oxychlorides or oxysulfates are formed. ( Compatible phases in hydraulic binders that are stable provided the concrete is dense and water kept out.)
As a result of the above the rusting of reinforcement does not proceed to the same extent.
Cracking or spalling due to rust does not occur

## Slide 132: Reducing Cracking Related to Autogenous Shrinkage
The autogenous deformation of concrete is defined as the unrestrained, bulk deformation that occurs when concrete is kept sealed and at a constant temperature.
Main cause is stoichiometric or chemical shrinkage.
  whereby the reaction products formed during the hydration of cement occupy less space than the corresponding reactants1. And/or
  Chemical demand for water for continued hydration of PC
A dense cement paste hydrating under sealed conditions will therefore self-desiccate creating empty pores within developing structure. If external water is not available to fill these “empty” pores, considerable shrinkage can result.
  1Le Chatelier H. Sur les changements de volume qui accompagnent Ie durcissement des ciments. Bulletin de la Societe d'Encouragement pour I'Industrie Nationale 1900:54-7.

## Slide 133: Reducing Cracking Related to Autogenous Shrinkage
Autogenous shrinkage does not occur in high strength tec-cement concretes because:
  The Brucite hydrates that form desiccate back to Brucite delivering water in situ for more complete hydration of Portland cement.
Mg(OH)2.nH2O (s) ↔ MgO (s) + H2O (l)
    As Brucite is a relatively weak mineral is compressed and densifies the microstructure.
  The stoichiometric shrinkage of Portland cement (first observed by Le Chatelier) is compensated for by the stoichiometric expansion of magnesium oxide on hydration.
    MgO (s) + H2O (l) ↔ Mg(OH)2.nH2O (s)
    40.31 + 18.0 ↔ 58.3 molar mass (at least!)
    11.2 + liquid ↔ 24.3 molar volumes (at least 116% expansion, probably more initially before desiccation as above!)

## Slide 134: More Complete Hydration of PC
Brucite consists of polar bound layers of ionically bound atoms
Strongly differentially charged surfaces and polar bound water account for many of the properties of Brucite
Brucite hydrates consist of polar bound layers of ionically bound atoms
NB. We think this loosely bound polar water is available for the more complete hydration of PC.
In most concrete 18-23% of the PC used never hydrates. If all the PC used could be made to hydrate less could be used saving on emissions be around 20%.
2C3S+7H => C3S2H4 + 3CH
2C2S+5H => C3S2H4 + CH

## Slide 135: Greater Density – Lower Permeability
Concretes have a high percentage (around 18% – 22%) of voids.
On hydration magnesia expands >=116.9 % filling voids and surrounding hydrating cement grains => denser concrete.
On carbonation to nesquehonite Brucite expands 308% sealing the surface.
Lower voids:paste ratios than water:binder ratios result in little or no bleed water, lower permeability and greater density.

## Slide 136: Reduced Permeability
As bleed water exits ordinary Portland cement concretes it creates an interconnected pore structure that remains in concrete allowing the entry of aggressive agents such as SO4--, Cl- and CO2
TecEco tec - cement concretes are a closed system. They do not bleed as excess water is consumed by the hydration of magnesia.
  As a result TecEco tec - cement concretes dry from within, are denser and less permeable and therefore stronger more durable and less permeable. Cement powder is not lost near the surfaces. Tec-cements have a higher salt resistance and less corrosion of steel etc.

## Slide 137: Densification During the Plastic Phase
Water
Log time
Observable Characteristic
Relevant Fundamental
Voids
Binder + supplementary cementitious materials
Hydrated Binder Materials
High water for ease of placement
Less water for strength and durability
Variables such as % hydration of mineral, density, compaction, % mineral H20 etc.
Consumption of water during plastic stage
Unhydrated Binder
Water is required to plasticise concrete for placement, however once placed, the less water over the amount required for hydration the better. Magnesia consumes water as it hydrates producing solid material.
Less water results in increased density and concentration of alkalis - less shrinkage and cracking and improved strength and durability.

## Slide 138: Durability - Reduced Salt & Acid Attack
Brucite has always played a protective role during salt attack. Putting it in the matrix of concretes in the first place makes sense.
Brucite does not react with salts once set* because it is a least 5 orders of magnitude less soluble, mobile or reactive.
  Ksp Brucite = 1.8 X 10-11
  Ksp Portlandite = 5.5 X 10-6
TecEco cements are more acid resistant than Portland cement
  This is because of the relatively high acid resistance (?) of Lansfordite and nesquehonite compared to calcite or aragonite
* Salts are eliminated in the wet stage by reaction with Mg++

## Slide 139: Substitution by Brucite => Long Term pH control
TecEco add reactive magnesia which hydrates forming Brucite which is another alkali, but much less soluble, mobile or reactive than Portlandite.
Brucite provides long term pH control.

## Slide 140: Carbonation is Eliminated in Tec-Cement Concretes
Consider what happens when Portlandite carbonates:
    Ca(OH)2 + CO2  CaCO3
    74.08 + 44.01 ↔ 100 molar mass
    33.22 + gas ↔ 28.10 molar volumes
  18.22% shrinkage
  Surface shrinkage causing cracks to appear.
In a concrete containing rMgO Consider nesquehonite the main phase:
MgO + H2O <=> Mg(OH)2 + CO2 + 2H2O <=> MgCO3.3H2O
40.31+ liquid <=> 58.31 + gas <=> 138.36 molar mass (at least!)
11.2 + liquid <=> 24.29 + gas <=> 74.77 molar volumes (at least!)
668% expansion relative to MgO or 308 % expansion relative to Mg(OH)2 (ex water or gas volume reduction)
Significant surface tightening stopping the process

## Slide 141: Reduced Steel Corrosion
Steel remains protected with a passive oxide coating of Fe3O4 above pH 8.9.
A pH of over 8.9 is maintained by the equilibrium Mg(OH)2 ↔ Mg++ + 2OH- for much longer than the pH maintained by Ca(OH)2 because:
  Brucite does not react as readily as Portlandite resulting in reduced carbonation rates and reactions with salts.
Concrete with Brucite in it is denser and carbonation is expansive, sealing the surface preventing further access by moisture, CO2 and salts.
Brucite is less soluble and traps salts as it forms resulting in less ionic transport to complete a circuit for electrolysis and less corrosion.
Free chlorides and sulfates originally in cement and aggregates are bound by magnesium
  Magnesium oxychlorides or oxysulfates are formed. ( Compatible phases in hydraulic binders that are stable provided the concrete is dense and water kept out.)

## Slide 142: Corrosion Reduced by a Lower More Stable Long Term pH
Eh-pH or Pourbaix Diagram The stability fields of hematite, magnetite and siderite
in aqueous solution; total dissolved carbonate = 10-2M.
In TecEco cements the long term pH is governed by the low solubility and carbonation rate of Brucite and is much lower at around 10.5 -11, allowing a wider range of aggregates to be used, reducing problems such as AAR and etching. The pH is still high enough to keep Fe3O4 stable in reducing conditions.
Steel corrodes below 8.9
Equilibrium pH of Brucite and of lime

## Slide 143: Less Freeze - Thaw Problems
Denser concretes do not let water in.
Brucite will to a certain extent take up internal stresses
When magnesia hydrates it expands into the pores left around hydrating cement grains:
MgO (s) + H2O (l) ↔ Mg(OH)2 (s)
40.31 + 18.0 ↔ 58.3 molar mass
11.2 + 18.0 ↔ 24.3 molar volumes
39.20 ↔ 24.3 molar volumes
At least 38% air voids are created in space that was occupied by magnesia and water!
Air entrainment can also be used as in conventional concretes
TecEco concretes are not attacked by the salts used on roads

## Slide 144: Rosendale Concretes - Implied Proof
Rosendale cements contained 14 – 30% MgO
A major structure built with Rosendale cements commenced in 1846 was Fort Jefferson near key west in Florida.
Rosendale cements were recognized for their exceptional durability, even under severe exposure. At Fort Jefferson much of the 150 year-old Rosendale cement mortar remains in excellent condition, in spite of the severe ocean exposure and over 100 years of neglect. Fort Jefferson is nearly a half mile in circumference and has a total lack of expansion joints, yet shows no signs of cracking or stress. The first phase of a major restoration is currently in progress.
More information from http://www.rosendalecement.net/rosendale_natural_cement_.html

## Slide 145: Many Issues with Concrete are Actually Mineralogical Issues caused by the Flawed Composition of Portland cement
They are usually resolved by “band aid” engineering fixes. e.g.
  Use of calcium nitrite, silanes, cathodic protection or stainless steel to prevent corrosion.
  Use of coatings to prevent carbonation.
  Crack control joins to mitigate the affects of shrinkage cracking.
  Plasticisers to improve workability.
Gypsum Portlandite and water are associated with many of the weaknesses of concrete
  TecEco would like to replace gypsum by reactive magnesia (rMgO)
  TecEco remove Portlandite and replace it with rMgO which hydrates to Brucite.
  The hydration of magnesia consumes significant water, prevents loss of bleed water and provides water for the more complete hydration of PC

## Slide 146: Problems with Portland Cement Fixed
Strength Faster & greater strength development especially with added pozzolans | Water removal by magnesia as it hydrates in tec-cements may result in a higher short term pH and therefore more affective pozzolanic reactions. Magnesia also acts as an accelerator for Pozzolanic reactions Increased proton strength/number due to stronger polarity caused by Mg++ => faster dissolution of SCM’s Brucite hydrate fills pore spaces taking up mix and bleed water as it hydrates reducing voids and shrinkage (Brucite hydrate is > 44.65 mass% water!). Greater density (lower voids:paste ratio) and lower permeability results in greater strength? Possible formation of Mg Al hydrates? Strength from self compaction

## Slide 147: Problems with Portland Cement Fixed (1)
Durability and Performance Permeability and Density Sulphate and chloride resistance Carbonation Corrosion of steel and other reinforcing | TecEco Tec - Cements are Denser and much less permeable Due mainly to the removal of water by magnesia and associated volume increases Surface tightening during carbonation of Mg phases Protected by Brucite Which is 5 times less reactive than Portlandite Not attacked by salts, Expansive carbonation of Brucite prevents overall carbonation Protective of steel reinforcing which does not corrode due to maintenance of long term pH.

## Slide 148: Problems with Portland Cement Fixed (2)
Durability and Performance Ideal lower long term pH Delayed reactions (e.g. alkali aggregate and delayed ettringite) | As Portlandite is removed The pH becomes governed by the pH of CSH and Brucite and Is much lower at around 10.5 -11 Stabilising many heavy metals and Allowing a wider range of aggregates to be used without AAR problems. Reactions such as carbonation are slower and The pH remains high enough to keep Fe3O4 stable for much longer. Internal delayed reactions are prevented Dry from the inside out and Have a lower long term pH

## Slide 149: Problems with Portland Cement Fixed (3)
Shrinkage Cracking, crack control | Net shrinkage is reduced due to: Stoichiometric expansion of magnesium minerals, and Reduced water loss.
Rheology Workability, time for and method of placing and finishing | The Mg++ ion adds a shear thinning making TecEco cements very workable. Hydration of magnesia rapidly adds early strength for finishing.

## Slide 150: Problems with Portland Cement Fixed (4)
Improved Properties | TecEco cements Can have insulating properties High thermal mass and Low embodied energy. Many formulations can be reprocessed and reused. Brucite bonds well and reduces efflorescence.
Properties (contd.) Fire Retardation | Brucite, hydrated magnesium carbonates are fire retardants TecEco cement products put out fires by releasing CO2 or water at relatively low temperatures.
Cost | No new plant and equipment are required. With economies of scale TecEco cements should be cheaper

## Slide 151: Problems with Portland Cement Fixed (5)
Sustainability issues Emissions and embodied energies | Tec, Eco and Enviro-Cements Less binder is required for the same strength Use a high proportion of recycled materials Immobilise toxic and hazardous wastes Can use a wider range of aggregates reducing transport emissions and Have superior durability. Tec-Cements Use less cement for the same strength Eco-Cements reabsorb chemically released CO2.

## Slide 152: Back to Science
There are too many non - scientific dogmas in the cement and concrete industry.
At TecEco we have relied on science to explain what we observe.
By using science rather than applying dogma it is easier
  to understand what is really happening.
  see a way forward for improvement.
Hydraulic cements like Portland cement will survive but changes including carbon capture and reformulation are essential for humanity to survive.

## Slide 153: TecEco Binder Theory – Better Cements
Tec-Cements
  Portlandite (Ca(OH)2) is too soluble, mobile and reactive.
    It carbonates, reacts with Cl- and SO4- and being soluble can act as an electrolyte.
  TecEco add reactive magnesia (rMgO)
    which hydrates, consuming significant water and concentrating alkalis forming Brucite which is another alkali, but much less soluble, mobile or reactive than Portlandite.
    Brucite regulates the long term pH
    With the use of rMgO
      Gypsum should not be used as rMgO +/- classified SCM’s will prevent flash setting (test).
        Too many problems associated with gypsum..
      SCM’s in particular classified SCM’s should be included to consume lime in the pozzolanic reaction and densify. (Strength and durability).
      Limestone should not be used.
  Carbon capture and reuse as aggregate is essential
Eco-cements
  Require appropriate particle packing so they are gas permeable
  Brucite and Portlandite carbonates.

## Slide 154: TecEco Patents – The Fine Print
Our patents cover reactive magnesia (rMgO, calcined at less than about 750 deg. C) included in a hydraulic composition with or without added pozzolans. They may or may not carbonate.
We define in most jurisdictions hydraulic cements according to the ASTM C219-94 definition as “a cement that sets and hardens by chemical interaction with water and that is capable of doing so under water”
In most jurisdictions we include slag cements as hydraulic and notice the American Slag Association think likewise. We therefore consider blending of slag with rMgO a blatant breach of our IP.
It is not advisable for cements to contain more than 5% non reactive magnesia because of dimensional distress (EN197-1, ASTM C-150) . Those companies already selling unspecified magnesia into the industry to blend with PC in proportions higher than 5% are therefore also breaching our ip.
We discuss the addition of aluminium in mixes in our patent and therefore have the prior art in relation to such additions.
We issue a warning to the dozen or more universities and companies out there that we know about that think they will get away with it. It does not pay to steal and I believe strongly in the property rights of ip.