## Slide 1: Greening Concrete – The Role of Reactive Magnesia.

## Slide 2: Global Carbon Flows
The global CO2 budget is the balance of CO2 transfers to and from the atmosphere. The transfers shown below represent the CO2 budget after removing the large natural transfers (shown to the right) which are thought to have been nearly in balance before human influence.
Global Carbon Flows After: David Schimel and Lisa Dilling, National Centre for Atmospheric Research 2003
Atmospheric increase | = | Emissions from fossil fuels | + | Net emissions from changes in land use | - | Oceanic uptake | - | Missing carbon sink
3.2 (±0.2) |  | 6.3 (±0.4) |  | 2.2 (±0.8) |  | 2.4 (±0.7) |  | 2.9 (±1.1)
From: Haughton, R., Understanding the Global Carbon Cycle. 2009, Woods Hole Institute at http://www.whrc.org/carbon/index.htm
Woods Hole Carbon Equation (In billions of metric tonnes)

## Slide 3: Net Atmospheric Increase in Terms of Billions of Tonnes CO2
Atmospheric increase | = | Emissions from fossil fuels | + | Net emissions from changes in land use | - | Oceanic uptake | - | Missing carbon sink
3.2 (±0.2) |  | 6.3 (±0.4) |  | 2.2 (±0.8) |  | 2.4 (±0.7) |  | 2.9 (±1.1)
Converting to tonnes CO2 in the same units by multiplying by 44.01/12.01, the ratio of the respective molecular weights.
Atmospheric increase | = | Emissions from fossil fuels | + | Net emissions from changes in land use | - | Oceanic uptake | - | Missing carbon sink
11.72 (±0.2) |  | 23.08 (±0.4) |  | 8.016 (±0.8) |  | 8.79 (±0.7) |  | 10.62 (±1.1)
From the above the annual atmospheric increase of CO2 is in the order of 12 billion metric tonnes.
Using the Figures from Woods Hole on the Previous Slide

## Slide 4: Natural Carbon Sinks
Carbon Sinks and Anthropogenic Actual and Predicted Consumption of Carbon
Modified from Figure 2 in Ziock, H. J. and D. P. Harrison. "Zero Emission Coal Power, a New Concept." from http://www.netl.doe.gov/publications/proceedings/01/carbon_seq/2b2.pdf. by the inclusion of a bar to represent sedimentary sinks.

## Slide 5: Energy Costs
Source: American Coal Council

## Slide 6: CO2 Or Energy ?

## Slide 7: Embodied Energy of Building Materials
Downloaded from www.dbce.csiro.au/ind-serv/brochures/embodied/embodied.htm (last accessed 07 March 2000)
Concrete is relatively environmentally friendly and has a relatively low embodied energy

## Slide 8: Average Embodied Energy in Buildings
Downloaded from www.dbce.csiro.au/ind-serv/brochures/embodied/embodied.htm (last accessed 07 March 2000)
Because so much concrete is used there is a huge opportunity for sustainability by reducing the embodied energy, reducing the carbon debt (net emissions) and improving properties that reduce lifetime energies.
Most of the embodied energy in the built environment is in concrete.

## Slide 9: Embodied Energy & Emmissions
Source: TecEco LCA Model

## Slide 10: Why Nothing Changes

## Slide 11: Remember
The Technology Paradigm defines what is or is not a resource.
Mg++ is a little ion with a big charge. It is the most powerful new tool in cement chemistry and most of the chemical and physical properties it imparts stem from this fact.
Don’t just do things. Your brain is the most powerful tool you have. Think about how you can do things better all the time.

## Slide 12: Mg Cements
Eco-Cements have relatively high proportions of magnesia which in permeable materials carbonates adding strength and durability. Eco-Cement formulations are generally used for bricks, blocks, pavers, pervious pavements and other permeable cement based products. See http://www.tececo.com/products.eco-cement.php
Enviro-Cements are made using large quantities of reactive magnesia which reacts to form brucite. Brucite is unique to TecEco Cements and is an ideal mineral for trapping toxic and hazardous wastes due to its layered structure, equilibrium pH level, durability and low solubility. See http://www.tececo.com/products.enviro-cement.php
Tec-Cements are cement blends that comprise of a hydraulic cement such as Portland cement mixed with a relatively small proportion of reactive magnesia and pozzolans and/or supplementary cementitious materials which react with Portlandite removing it and making more cement or are activated by Portland cement. They offer a solution to many of the technical problems that plague traditional cement formulations caused by the reactivity of lime (Portlandite) and have significant advantages including faster setting even with a high proportion of non PC additions. See http://www.tececo.com/products.tec-cement.php
Others Mg - Phosphate cements, Sorel type cements and others

## Slide 13: TecEco Cements Strength with Blend and Permeability
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 29 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31
 | 100 | 117 | 120 | 117 | 110 | 100 | 85 | 80 | 78 | 78 | 77 | 76 | 75 | 74 | 73 | 73 | 72 | 72 | 71 | 71 | 70 | 70 | 69 | 69 | 69 | 68 | 68 | 68 | 67 | 67
 | 100 | 112 | 117 | 112 | 105 | 85 | 70 | 62 | 56 | 52 | 49 | 47 | 45 | 44 | 43 | 42 | 42 | 42 | 42 | 42 | 42 | 41 | 41 | 41 | 40 | 40 | 40 | 40 | 40 | 39
 | 100 | 107 | 110 | 107 | 100 | 80 | 65 | 55 | 45 | 37 | 32 | 26 | 24 | 23 | 22 | 21 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20
High OPC
High Magnesia
High Permeability
Strength on Arbitrary Scale 1-100
Tec-cement concretes
Eco-cement concretes
Enviro-cement concretes
Mg -> High molar volume growth
Ideal microstructure
Bonding
Stability
Ideal pH for wastes immobilisation
Sequestration

## Slide 14: The Concept of a Carbonate Built Environment
John Harrison from TecEco has for many years been advocating the carbonate built environment solution to global warming
13th July 2002 – Fred Pearce in New Scientist about TecEco magnesium cement technology:
“THERE is a way to make our city streets as green as the Amazon rainforest. Almost every aspect of the built environment, from bridges to factories to tower blocks, and from roads to sea walls, could be turned into structures that soak up carbon dioxide- the main greenhouse gas behind global warming. All we need to do is change the way we make cement.
All we have to do is change the way we do things and do what a big old tree does – make our homes out of CO2.

## Slide 15: How Much Man Made Carbonate to Neutralise our Emmissions?
MgO + H2O => Mg(OH)2 + CO2 + 2H2O => MgCO3.3H2O 40.31 + 18(l) => 58.31 + 44.01(g) + 2 X 18(l) => 138.368 molar masses. 44.01 parts by mass of CO2 ~= 138.368 parts by mass MgCO3.3H2O 1 ~= 138.368/44.01= 3.144 12 billion tonnes CO2 ~= 37.728 billion tonnes of nesquehonite
or
MgO + H2O => Mg(OH)2 + CO2 + 2H2O => MgCO3 40.31 + 18(l) => 58.31 + 44.01(g) + 2 X 18(l) => 84.32 molar masses. CO2 ~= MgCO3 44.01 parts by mass of CO2 ~= 84.32 parts by mass MgCO3 1 ~= 84.32/44.01= 1.9159 12 billion tonnes CO2 ~= 22.99 billion tonnes magnesite
CaO + H2O => Ca(OH)2 + CO2 + 2H2O => CaCO3 56.08 + 18(l) => 74.08 + 44.01(g) + 2 X 18(l) => 100.09 molar masses. CO2 ~= CaCO3 44.01 parts by mass of CO2 ~= 100.09 parts by mass MgCO3 1 ~= 100.09/44.01= 2.274 12 billion tonnes CO2 ~= 27.29 billion tonnes calcite (limestone)
If a proportion of the built environment were man made carbonate, how much would we need to reverse global warming?

## Slide 16: The Potential for Man Made Carbonates in Concretes
Chart: 
Assumptions - 50% non PC N-Mg mix and Substitution by Mg Carbonate Aggregate |  | 
Percentage by Weight of Cement in Concrete | 15.00% | 
Percentage by weight of MgO in cement | 6% | 
Percentage by weight CaO in cement | 29% | 
Proportion Cement Flyash and/or GBFS | 50% | 
1 tonne Portland Cement | 0.864 | Tonnes CO2
Proportion Concrete that is Aggregate | 72.5% | 
CO2 captured in 1 tonne aggregate | 1.092 | Tonnes CO2
CO2 captured in 1 tonne MgO (N-Mg route) | 2.146 | Tonnes CO2
CO2 captured in 1 tonne CaO (in PC) | 0.785 | Tonnes CO2
With carbon trading think of the potential for sequestration (=money with carbon credits) making man made carbonate aggregate
Source USGS: Cement Pages

## Slide 17: Man Made Carbonate Sequestration
Chart: BAU Emissions ~ Target and Achieved
| 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024 | 2025 | 2026 | 2027 | 2028 | 2029 | 2030
BAU Emissions Scenario Selected (EIA A,B,C,D) | 26693.9288 | 27316.0214 | 27938.1141 | 28560.2068 | 29182.2995 | 29804.3922 | 30426.4849 | 31048.5776 | 31670.6702 | 32292.7629 | 32914.8556 | 33536.9483 | 34159.041 | 34781.1337 | 35403.2264 | 36025.319 | 36647.4117 | 37269.5044 | 37891.5971 | 38513.6898 | 39135.7825 | 39757.8752 | 40379.9678 | 41002.0605 | 41624.1532 | 42246.2459
Calculated Target Sequestration Required (based on emissions scenario A) | 0 | 10.1398 | 27.9043 | 76.1243 | 204.5549 | 535.5493 | 1342.2991 | 3138.4591 | 6626.9596 | 12255.7351 | 19549.4856 | 27129.1159 | 33667.1446 | 38622.4212 | 42133.0347 | 44590.8346 | 46367.7838 | 47732.4358 | 48856.3395 | 49842.4759 | 50750.6566 | 51615.0032 | 52454.7903 | 53280.8459 | 54099.2335 | 54913.3427
CO2 Sequestered as MgCO3 in Built Environment (Given % Man Made Carbonate & Adoption Period) | 0 | 2.3995 | 6.7711 | 18.9905 | 52.679 | 143.3214 | 377.1225 | 939.1467 | 2148.5381 | 4368.7306 | 7702.8165 | 11733.6155 | 15745.8594 | 19220.5485 | 22025.9096 | 24276.2915 | 26151.4629 | 27806.3979 | 29350.6289 | 30855.0517 | 32363.8966 | 33904.604 | 35494.531 | 37145.1465 | 38864.5529 | 40658.9723
Scenario A chosen
See the TecEco Sequestration Model at http://www.tececo.com/files/spreadsheets/GaiaEngineeringVGeoSequestrationV1.3_5May09.xls

## Slide 18: Man Made Carbonate Sequestration Can Solve the Problem
Chart: Mass CO2 in the Atmosphere
See the TecEco Sequestration Model at http://www.tececo.com/files/spreadsheets/GaiaEngineeringVGeoSequestrationV1.3_5May09.xls

## Slide 19: What Carbonate?
The following table lists principal metal oxides of Earth's Crust. Theoretically up to 22% of this mineral mass is able to form carbonates.
Table Source: http://en.wikipedia.org/wiki/Carbon_sequestration
Oxide | Percent of Crust | Carbonate | Enthalpy change (kJ/mol) | Comment
SiO2 | 59.71 |  |  | Too difficult
Al2O3 | 15.41 |  |  | Too difficult
CaO | 4.90 | CaCO3 | -179 | Feasible
MgO | 4.36 | MgCO3 | -117 | Feasible
Na2O | 3.55 | Na2CO3 |  | Too soluble
FeO | 3.52 | FeCO3 |  | Too difficult
K2O | 2.80 | K2CO3 |  | Too soluble
Fe2O3 | 2.63 | FeCO3 |  | Too difficult
 | 21.76 | All Carbonates |  | 

## Slide 20: Magnesium Carbonates
Seawater Reference Data | g/l H20 | Cation radius (pm)
Chloride (Cl--) | 19 | 167
Sodium (Na+) | 10.5 | 116
Sulfate (S04--) | 2.7 | ?
Magnesium (Mg++) | 1.29 | 86
Calcium (Ca++) | 0.412 | 114
Potassium (K+) | 0.399 | 152
Because of the low molecular weight of magnesium, it is ideal for scrubbing CO2 out of the air and sequestering the gas into the built environment:
More CO2 is captured than in calcium systems as the calculations below show.
At 2.09% of the crust magnesium is the 8th most abundant element
Sea-water contains 1.29 g/l compared to calcium at .412 g/l. Many brines contain much more.
Magnesium compounds have low pH and polar bond in composites making them suitable for the utilisation of other wastes.

## Slide 21: Morphology Microstructure & Molar Volume Growth
Mineral (or Product) | Formula | Molar Vol ume | Growth relative to MgO | Hard ness | Habit | Conditions of Formation | Type
Brucite | Mg(OH)2 | 24.63 |  | 2.5 - 3 | Blocky pseudo hexagonal chrystals. |  | Brucite
Brucite Hydrates | Mg(OH)2.nH2O | ? |  |  | Not much known about them! |  | Brucite Hydrates
Pokrovskite | Mg 2 (CO 3 )(OH) 2 · 0.5(H 2 O) |  |  | 3 |  |  | ?
Artinite | Mg2(CO3)(OH)2•3(H2O) | 96.43 | 291% | 2.5 | Bright, white acicular sprays |  | Basic
Hydromagnesite Giorgiosite | Mg5(CO3)4(OH)2.4H2O | 211.11 | 756% | 3.5 | Include acicular, lathlike, platy and rosette forms |  | Basic
Dypingite | Mg5(CO3)4(OH)2·5H2O |  |  | ? | Platy or rounded rosettes | Low CO2, H2O | Basic
Magnesite | MgCO3 | 28.02 | 13% | 3.9 | Usually massive |  | Magnesite
Barringtonite | MgCO3·2H2O |  |  | 2.5 | Glassy blocky crystals |  | Magnesite Di Hydrate
Nesquehonite | MgCO3·3H2O | 75.47 | 206.41% | 2.5 | Acicular prismatic needles | Very Variable. Has been found on meteorites! | Magnesite Tri Hydrate
Lansfordite | MgCO3·5H2O | 103.47 | 320.09% | 2.5 | Glassy blocky crystals |  | Magnesite Penta Hydrate

## Slide 22: Why Nesquehonite for Man Made Carbonate?
Can be manufactured easily using the N-Mg Process at room temperature with little energy
Suitable shape to improve microstructure
Can be used directly in many products
  Accoustic panels, non structural panels, insulation etc.
Possible use directly or agglomerated in concrete as a man made aggregate
Stable over a wide PT range (See Ferrini et al )
Suitable source of Magnesium for manufacture of MgO
Nesquehonite has a low pH and polar bonds in composites making it suitable for the utilisation of other wastes
XRD Pattern Nesquehonite
Nesquehonite courtesy of Vincenzo Ferrini, university of Rome.
We have to ask ourselves why we are still digging holes in the ground. The industry would encounter far less bureaucratic blocking, make more money and go a long way towards solving global warming by manufacturing out of Mg, thin air and water its own inputs!
Mg++ + 3H2O + CO3-- => MgCO3·3H2O

## Slide 23: How Easy is Nesquehonite to Make? Thermodynamics and Kinetics
Enthalpy
Mg++ + CO3-- + 3H2O  MgCO3·3H2O (nesquehonite)
Hor = Hof (final) - Hof (initial)
Hor = {Hof (MgCO3·3H2O,s)} – {Hof (Mg++,aq) + Hof (CO3--,aq) + 3 X Hof (H2O,l)}
Hor = - 1977.26 - (- 466.85 - 393.51 - 3 X 241.81) kJ.mol-1
Hor = - 1977.26 + 1585.79
Hor = - 391.47 kJ.mol-1.
The reaction is exothermic with - 391.47 kJ.mol-1 liberated.
Gibbs Free Energy
Mg++ + CO3-- + 3H2O  MgCO3·3H2O (nesquehonite)
Gor = {Gof (MgCO3·3H2O,s)} - {Gof (Mg++,aq) + Gof (CO3--,aq) + 2 X Gof (H2O,l)}
Gor = - 1723.75 - (- 454.8 – 527.90 - 3 X 228.57) kJ.mol-1
Gor = - 51.34 kJ.mol-1
The reaction is spontaneous
Remaining Research Issues
How to remove unsuitable carbonates and other salts from a mixed brine or output. Disposal of by-products such as HCl. Existing patented solutions complex and involve energy.

## Slide 24: Structure of Nesquehonite
Stephan G W , MacGillavry C H , Acta Crystallographica, Section B , 28 (1972) p.1031-1033, The crystal structure of nesquehonite, MgCO3*3H2O
Infinite chains of MgO6 octahedra and CO3 groups hydrogen bonded together. Note that the atomic arrangement in nesquehonite shows no close relationship to those of the other known hydrated magnesium carbonates
Giester, G., Lengauer C. L. , and Rieck B. , The crystal structure of nesquehonite,
MgCO3.3H 2 O, from Lavrion, Greece, Mineralogy and Petrology (2000) 70: 153–163

## Slide 25: Manufacture of Nesquehonite (Tec-Kiln, N-Mg route)
Scope for Reducing Energy Using Waste Heat?
Initial weight loss below 100oC consists almost entirely of water (1.3 molecules per molecule of nesquehonite). Between 100 and 1500C volatilization of further water is associated with a small loss of carbon dioxide (~3-5 %).
From 1500C to 2500C, the residual water content varies between 0-6 and 0-2 molecules per molecule of MgC03. Above 3000C, loss of carbon dioxide becomes appreciable and is virtually complete by 4200C, leaving MgO with a small residual water content.
Energy could be saved using a two stage calcination process using waste energy for the first stage.
Dell, R. M. and S. W. Weller (1959). "The Thermal Decomposition of Nesquehonite MgCO3 3H20 And Magnesium Ammonium Carbonate MgCO3 (NH4)2CO3 4H2O." Trans Faraday Soc 55(10): 2203 - 2220.

## Slide 26: Gaia Engineering
MgCO3.3H2O
N-Mg Process
NH4Cl or HCl
Industrial CO2
MgO
TecEco Tec-Kiln
Eco-Cements
Building components & aggregates
TecEco Cement Manufacture
CaO
Clays
Portland Cement Manufacture
Brine, Sea water, Oil Process water, De Sal Waste Water etc .
Tec-Cements
Other wastes
Fresh Water
GBFS
Fly ash
www.gaiaengineering.com and www.tececo.com

## Slide 27: Moleconomic Flows – N-Mg Process The Nesquehonite Route
The annual world production of HCl is about 20 million tons, most of which is captive (about 5 million tons on the merchant market).

## Slide 28: The Tec-Reactor Hydroxide Carbonate Capture Cycle
The solubility of carbon dioxide gas in seawater
  Increases as the temperature approached zero and
  Is at a maxima around 4oC
This phenomenon is related to the chemical nature of CO2 and water and
Can be utilised in a carbonate – hydroxide slurry process to capture CO2 out of the air and release it for storage or use in a controlled manner

## Slide 29: The N-Mg Process
Tec-Kiln
NH3 and a small amount of CO2
MgCO3.3H2O
MgO
MgO
Mg(OH)2
CO2
H2O
Steam
NH4Cl and a small amount of NH4HCO3
Filter
Filter
Mg rich water
Ammoniacal Mg rich water
MgCO3.3H2O
HCl
A Modified Solvay Process for Nesquehonite
The process is not dissimilar to the conventional softening of water using sodium carbonates and bicarbonates

## Slide 30: The TecEco Tec-Kiln
An obvious future requirement will be to make cements without releases so TecEco are developing a top secret kiln for low temperature calcination of alkali metal carbonates and the pyro processing and simultaneous grinding of other minerals such as clays.
The TecEco Tec-Kiln makes no releases and is an essential part of TecEco's plan to sequester massive amounts of CO2 as man made carbonate in the built environment .
The TecEco Tec-Kiln has the following features:
Operates in a closed system and therefore does not release CO2 or other volatiles substances to the atmosphere
Can be powered by various potentially cheaper non fossil sources of energy such as intermittent solar or wind energy.
Grinds and calcines at the same time thereby running 25% to 30% more efficiently.
Produces more precisely definable product. (Secret as disclosure would give away the design)
The CO2 produced can be sold or re-used in for example the N-Mg process.
Cement made with the Tec-Kiln will be eligible for carbon offsets.
To further develop the Tec-Kiln, TecEco require not only additional funding but also partners able to provide expertise.

## Slide 31: Carbon Capture During Manufacture MgO
Eco-Cement – With Capture during Manufacture
Eco-Cement – No Capture during Manufacture
CO2
CO2 from atmosphere
CO2 capture (Back to N – Mg Process etc.)
Carbon neutral except for carbon from process emissions
Net sequestration less carbon from process emissions
Use of non fossil fuels => Low or no process emissions
MgO
MgO
Mg(OH)2
H2O
H2O
H2O
Mg(OH)2
MgCO3.3H2O
H2O
H2O
H2O
MgCO3.3H2O

## Slide 32: Gaia Engineering - An Industrial TecEcology!
N-Mg Process
TecEco Tec-Kiln
CO2
Nesquehonite
Nichromet Process
TecEco Cements
Direct Products
http://www.nichromet.com
http://www.tececo.com
Reactive MgO

## Slide 33: Geomimicry
Carbonate sediments such as these cliffs represent billions of years of sequestration and cover 7% of the crust.
There are 1.2-3 grams of magnesium and about .4 grams of calcium in every litre of seawater.
There is enough calcium and magnesium in seawater with replenishment to last billions of years at current needs for sequestration.
To survive we must build our homes like these seashells using CO2 and alkali metal cations. This is geomimicry

## Slide 34: Geomimicry
Sequestering carbon in calcium and magnesium carbonate materials and other wastes in the built environment as in Gaia Engineering mimics nature in that carbon is used in the homes or skeletal structures of most plants and animals.
In eco-cement concretes the binder is carbonate and the aggregates are preferably carbonates and wastes. This is “geomimicry”
CO2
C
CO2
Waste
CO2
CO2
Pervious pavement

## Slide 35: Future Cement Contenders Mg Group
Cements Based on | Process | Process CO2 (tonnes CO2 / tonne Compound) | Decarbonation CO2 (tonnes CO2 / tonne Compound) | Emissions (if no kiln capture– tonnes CO2 / tonne Compound) | Absorption (tonnes CO2 / tonne Compound, Assuming 100% carbonation) | Net Emissions (Sequestration) (tonnes CO2 / tonne Compound, Assuming 100% carbonation) | Example of Cement Type | Apply to | Comment | Notes
MgO 750-1000oC | Conventional | .403 | 1.092 | 1.495 | -1.092 | .403 | Sorel & Magnesium Phosphate cements. | Historic and Conventional Oak Ridge spin offs. | Mg Phosphates potentially v. green. | 1
<750oC | MgCO3 + Tec-Kiln | .056 |  | .056 | -1.092 | -1.036 | Eco-cement concrete, pure MgO concretes Novacem concretes | TecEco, Cambridge & Novacem | TecEco Eco-Cement Force carbonated pure MgO | 1
<450oC | MgCO3.3H2O Conventional | .693 | 1.092 | 1.784 | -2.184 | -.399 | Eco-cement concrete, pure MgO concretes Novacem concretes? | TecEco, Cambridge & Novacem | Mg Solvay process University of Rome, initial absorption is 1.092 | 1
<450oC | MgCO3.3H2O +Tec-Kiln | .038 |  | .038 | -2.184 | -2.146 | Eco-cement concrete, pure MgO concretes Novacem concretes? | TecEco, Cambridge & Novacem | N-Mg route University of Rome | 1
Modified Ternary Blends (50% PC) | Split Process – Lime (with capture)then clinker | .185 |  | .185 | .002 | .183 | Terniary mix with MgO additive. | Most dense concretes |  | 2
http://www.tececo.com/files/spreadsheets/TecEcoCementLCA20Jan2011.xls

## Slide 36: Wastes
From waste to resource: 2006 world waste survey
Elisabeth Lacoste, Philippe Chalmin, Cercle Cyclope, Veolia Environmental Services, Economica (Firm)

## Slide 37: Wastes in Mg-Cement Composites?
Cellulosic fiber
Bonded Wood fiber – nesquehonite composites
+
Nesquehonite
Physical entanglement and polar bonding
Wastes adding value to mineral composites because of their physical and chemical properties

## Slide 38: Use of Wastes in Tec, Eco and Enviro Cements
In a Portland cement brucite matrix
  PC takes up lead, some zinc and germanium
  Magnesium minerals are excellent hosts for toxic and hazardous wastes.
  Heavy metals not taken up in the structure of Portland cement minerals or trapped within the brucite layers end up as hydroxides with minimal solubility.
The brucite in TecEco cements has a structure comprising electronically neutral layers and is able to accommodate a wide variety of extraneous substances between the layers and cations of similar size substituting for magnesium within the layers and is known to be very suitable for toxic and hazardous waste immobilisation.
Layers of electronically neutral brucite suitable for trapping balanced cations and anions as well as other substances.
Salts and other substances trapped between the layers.
Van der waals bonding holding the layers together.

## Slide 39: Ideal Ph Regime in Tec-Cement Dense Concretes
There is a 104 difference

## Slide 40: TecEco Eco-Cements
Criteria | Good | Bad
Energy Requirements and Chemical Releases, Reabsorption (Sequestration?) | The MgO used could be made without releases and using the N-Mg route | 
Speed and Ease of Implementation | Easily implemented as no carbonation rooms etc reqd. | Permissions and rewards systems see http://www.tececo.com/sustainability.permissions_rewards.php.
Barriers to Deployment |  | We need cheaper MgO and carbon trading!
Cost/Benefit | Economies of scale issue for MgO to overcome | 
Use of Wastes? or Allow Use of Wastes? | A vast array of wastes can be incorporated | 
Performance |  | 
Engineering | Excellent | Need to be handled gently in the first few days
Thermal | Engineered thermal capacity and conductivity. | 
Architectural |  | 
Safety |  | 
Audience 1 |  | 
Audience 2 |  | 
Left: Recent Eco-Cement blocks made, transported and erected in a week. Laying and Eco-Cement floor. Eco-Cement mortar & Eco-cement mud bricks. Right: Eco-Cement permeacocretes and foamed concretes
Eco-Cements are blends of one or more hydraulic cements and relatively high proportions of reactive magnesia with or without pozzolans and supplementary cementitious additions. They will only carbonate in gas permeable substrates forming strong fibrous minerals. Water vapour and CO2 must be available for carbonation to ensue.
Eco-Cements can be used in a wide range of products from foamed concretes to bricks, blocks and pavers, mortars renders, grouts and pervious concretes such as our own permeacocrete. Somewhere in the vicinity of the Pareto proportion (80%) of conventional concretes could be replaced by Eco-Cement.

## Slide 41: Forced Carbonation ~ Optimisation
 | Forced Carbonation (Cambridge) | Kinetic Optimisation (TecEco)
Steps | Multistep process | Less steps = lower costs
Rate | Variable | Varying on weather conditions (wet dry best and gas permeability)
% Carbonation in 6 months | 70% (reported, could be more if permeable) | 100%
Ease of general implementation | Require point sources CO2 | Can be implemented very quickly
Can use large quantities of fine wastes | Can use large quantities of fine wastes like fly ash that are not necessarily pozzolanic | Fine wastes tend to reduce gas permeability
Safety | Are carbonation rooms safe? | No issues
Key requirements | Special carbonation rooms | Optimal kinetics including gas permeability
Physical rate considerations | Doubling the concentration of CO2 doubles the rate of carbonation. | Doubling the pore size quadruples the rate of carbonation.
Other issues | Able to be sealed with paint etc as pre carbonated | Some sealing paints will slow down carbonation
Forced carbonation of silicate phases as promoted by some is nonsense
According to ECN "The CO2 concentration in power station flue gas ranges from about 4% (by volume)for natural gas fired combined cycle plants to about 14% for pulverised coal fired boilers." At 10% the rate increase over atmospheric could be expected to be 10/.038 = 263 times provided other kinetic barriers such as the delivery of water do not set in. Ref: http://www.ecn.nl/en/h2sf/products-services/co2-capture/r-d-activities/post-combustion-co2-capture/ accessed 24 Mar 08.

## Slide 42: Carbonation Optimisation
Dissolution of MgO
  Gouging salts e.g MgSO4, MgCl2 and NaCl (Not used by TecEco)
  Various catalysing cations e.g. Ca ++ and Pb ++ and ligands EDTA, acetate, oxalate citrate etc. (Not used by TecEco)
  Low temperature calcination = Low lattice energy = high proportion of unsaturated co-ordination sites = rapid dissolution. See http://www.tececo.com/technical.reactive_magnesia.php
Carbonation – High concentration of CO3-- at high pH as a result of OH- from Portlandite
Possible catalysis and nucleation by polar surface of calcium silicate hydrate at high pH
Wet dry conditions. Wet for through solution carbonation, dry for gas transport.

## Slide 43: Why Nesquehonite in Concretes?
Significant molar volume expansion.
Excellent morphology. Nesquehonite has an ideal shape that contributes strength to the microstructure of a concrete
Forms readily at moderate and high pH in the presence of CSH. (Catalytic nucleation mechanism?)
Can be manufactured using the N-Mg Process
Can be agglomerated
Stable over a wide PT range (See Ferrini’s work)
The hydration of PC => alkalinity dramatically increasing the CO3-- levels that are essential for carbonation.
Captures more CO2 than Calcium
Ideal wet dry conditions are easily and cheaply provided. Forced carbonation is not required (Cambridge uni and others)
3H2O + CO3---- + Mg++ => MgCO3·3H2O
XRD Pattern Nesquehonite
Nesquehonite courtesy of Vincenzo Ferrini, university of Rome.
We have to ask ourselves why we are still digging holes in the ground. The industry would encounter far less bureaucratic blocking, make more money and go a long way towards solving global warming by manufacturing out of Mg, thin air and water its own inputs!
pH dependent speciation

## Slide 44: Porosity ~ Permeability

## Slide 45: Grading Eco-Cements
Simple Grading
Fineness Modulus or
Virtual Packing (TecEco preferred route – see next slide)
Chart: 
| 9.5 | 4.75 | 2.36 | 1.18 | 0.6 | 0.3 | 0.15 | <0.15
Combined % Retained | 0 | 0.17751 | 0.07364 | 0.13134 | 0.10279 | 0.087671 | 0.10688 | 0.10688
Upper | 0.01 | 0.3 | 0.2 | 0.2 | 0.2 | 0.2 | 0.135 | 0.07
Lower | 0 | 0.2 | 0.1 | 0.1 | 0.1 | 0.1 | 0.065 | 0.03
With Eco-Cements the idea is to imperfectly pack particles so that the percolation point is exceeded.

## Slide 46: TecSoft TecBatch
TecBatch is a unique scientifically based concrete batching tool that, when released, will identify and optimally batch a wide range of concretes for any purpose.
The software is not based on past experience with particular mixes as are many other batching programs. On the contrary, it but goes back to scientific principles, based on particle properties and packing to predict properties for each formulation. A User Data Feedback Scheme will ensure that the program will be continually improved over time.
TecBatch will be a powerful tool for design engineers and engineering students, concrete researchers and batching plant operators interested in improving the profitability, versatility and most importantly, the sustainability of concretes. It will be able to model any concrete, including those using the ground breaking TecEco Tec, Eco and Enviro environmentally sustainable cements.
The advanced algorithms in TecBatch will optimise the use of materials, minimise costs and increase profits. It will allow users to specify the properties desired for their concrete, then suggests optimal solutions. Virtual concrete will become a reality with TecBatch.
To further develop the TecBatch software, TecSoft require not only additional funding but also partners able to provide the programming expertise and testing capability. Further details

## Slide 47: Commercial Products Eco-Cement
TecEco Tec and Eco-Cement bricks, blocks and pavers are now being made commercially in Australia
We may be able to get a local manufacturer to make them for you.

## Slide 48: Economics of Magnesium Carbonate Binder Based Masonry Products
What this embedded spreadsheet demonstrates is that Magnesium Carbonate Block formulations are uneconomic unless the price of reactive MgO approaches that of PC or there is a high price for carbon or alternatively less MgO can be used!
Because of molar volume growth less can be used but we must still address supply chain issues.
This embedded spreadsheet looks only at the binder price and assumes all other factors remain the same

## Slide 49: Eco-Cement Mortars Renders and Mud Bricks
First Eco-cement mud bricks and mortars in Australia
  Tested up twice as strong as the PC controls
  Mud brick addition rate 2.5%
  Addition rate for mortars 1:8 not 1:3 because of molar ratio volume increase with MgO compared to lime.

## Slide 50: Eco-Cement Permeacocrete Pervious Pavements
“Why mix rainwater from heaven with pollution and call it storm water when you could sell it!”
John Harrison, B.Sc. B.Ec. FCPA

## Slide 51: Permeacocretes
Permeacocretes are an example of a product where the other advantages of using reactive MgO overcome its high cost and lack of a suitable market for carbon trading.
The use of MgO gives an ideal rheology which makes it possible to make permeacocrete pervious pavements using conventional road laying equipment therefore substantially reducing labour costs.
There are many other advantages of pervious pavements see http://www.tececo.com/files/conference%20presentations/TecEcoPresentationSGA25Mar2010.ppt

## Slide 52: Conclusion
Eco-Cements have a Supply Chain Problem
Unless
  We can reduce the price of reactive MgO
  Or introduce specialised MgO technologies with improved properties where the price of MgO does not negatively impact the bottom line

## Slide 53: Tec-Cements
Tec-Cements (5-20% MgO, 80-95% OPC)
  contain more Portland cement than reactive magnesia. Reactive magnesia hydrates in the same rate order as Portland cement forming Brucite which uses up excess water reducing the voids:paste ratio, increasing density and possibly raising the short term pH.
  Reactions with pozzolans are more affective. After much of the Portlandite has been consumed Brucite tends to control the long term pH which is lower and due to it’s low solubility, mobility and reactivity results in greater durability.
  Other benefits include improvements in density, strength and rheology, reduced permeability and shrinkage and the use of a wider range of aggregates many of which are potentially wastes without reaction problems.

## Slide 54: PC 50% Modified Ternary Mix with N-Mg Route Mg Carbonate Aggregate
TecEco announce a way forward to greater sustainability for the Portland cement industry.
Up to 30% or more strength at all stages with high replacement ternary mixes. (GBFS + fly ash replacing PC.)
Finishers can go home early using >50% replacement mixes removing the remaining barrier to their implementation
Brilliant rheology, low shrinkage and little or no cracking.
Excellent durability.
A solution to autogenous shrinkage?

## Slide 55: Results for TecEco 20 and 32 MPa Modified Ternary Mixes
Date of Trial Mix | 30/10/2010 20MPa |  | 3/12/2010 32MPa | 
Constituents | Kg | % | Kg | %
GP PC, kg/m3 | 116 | 47.93 | 155 | 47.78
Flyash, kg/m3 | 58 | 23.97 | 78 | 24.04
Slag, kg/m3 | 58 | 23.97 | 78 | 24.04
Reactive Magnesia, kg/m3 | 10 | 4.13 | 13.4 | 4.13
MgO relative to PC |  | 8.7 |  | 8.7
20mm, kg/m3 | 710 |  | 730 | 
10mm, kg/m3 | 275 |  | 280 | 
Total Coarse Aggregate | 985 |  | 1010 | 
Manufactured Sand, kg/m3 | 490 |  | 440 | 
Fine Sand, kg/m3 | 390 |  | 350 | 
Total Fine Aggregate | 880 |  | 790 | 
WR (WRDA PN), ml/100kg | 350 |  | 400 | 
Water, lt/m3 | 185 |  | 199 | 
Design Slump, mm | 80 |  | 100 | 
Actual Slump, mm | 80 |  | 100 | 
Strength | 20 Mpa |  | 32MPa | 
3 Day | 13.0 |  | 17.0 | 
7 Day | 18.0 |  | 24.5 | 
28 Day | 32.5 |  | 42.5 | 
56 Day | 39.0 |  | 46.5 | 
Shrinkage | 20 Mpa |  | 32MPa | 
1 week | 330 |  | 320 | 
2 week | 430 |  | 420 | 
3 week | 500 |  | 490 | 
4 week | 560 |  | 520 | 
7 week | 660 |  | 580 | 
Chart: 
| 3 Day | 7 Day | 28 Day | 56 Day
20 Mpa | 13 | 18 | 32.5 | 39
32MPa | 17 | 24.5 | 42.5 | 46.5
Chart: 
| 1 week | 2 week | 3 week | 4 week | 5 week | 6 week | 7 week
20 Mpa | 330 | 430 | 500 | 560 | 600 | 650 | 660
32MPa | 320 | 420 | 490 | 520 | 580
NB. Our patents in all countries define the minimum added % MgO as being >5% of hydraulic cement components or hydraulic cement components + MgO

## Slide 56: A Tec-Cement Modified Ternary Mix

## Slide 57: Tec-Cement Mixes
 | Ordinary Mixes | TecEco Tec-Cement Mixes | Notes
Reactive MgO as defined | None | Usually 8 to 10% / PC added | 1
Pozzolan (Pos) | Should be used | Recommended. | 
Supplementary cementitious materials (SCM’s) | Should be used | Recommended. | 2
Limit on additions pozzolans + SCM’s | Limited by standards that are increasingly exceeded | > 50% recommended especially if a ternary blend | 
Rheology | Usually sticky, especially with fly ash. Hard to finish. | Slippery and creamy. Easy to finish. | 
Setting time | Slow. Especially with flyash only. | Much faster. Blends with a high proportion Pos. and SCM’s set like ordinary PC concrete. | 
Shrinkage and cracking | Significant | Much less | 
Additives | Usually used | Not necessary | 
Durability | Without additions of Pos and SCM’s questionable. | Excellent especially with additions of Pos and SCM’s | 
28 day Strength (prev 20 MPA mix) | < .20 Mpa/Kg PC/m3 | > .27 Mpa/Kg PC/m3 | 
$ Cost Binder/Mpa at 28 days (prev 20 & 32 MPa mixes) | > ($2.30-$2.50) | < ($1.50-$1.90) | 3
Notes 1. See http://www.tececo.com/technical.reactive_magnesia.php. % is relative to PC and in addition to amount already in PC
2. To keep our patents simple we included supplementary cementitious materials as pozzolans in our specification
3. See economics pages following
We recommend using both Pos and SCM’s together

## Slide 58: Tec-Cement Hi Fly Ash Blends
Our Tec-Cement concrete tilt ups are free of plastic cracking, obvious bleed marking and other defects. Normal concrete in the middle

## Slide 59: Why Put Brucite in Dense Concretes?
Improved rheology (see http://www.tececo.com/technical.rheological_shrinkage.php)
Prevents shrinkage and cracking (see http://www.tececo.com/technical.rheological_shrinkage.php)
Provides pH and eH control. Reduced corrosion. Stabilises CSH when Ca++ consumed by the pozzolanic reaction (Encouraged) Stabilises wastes
Provides early setting even with added pozzolans or supplementary cementitios materials
Relinguishes polar bound water for more complete hydration of PC thereby preventing autogenous shrinkage?
Pourbaix diagram steel reinforcing
Surface charge on magnesium oxide
Equilibrium pH brucite

## Slide 60: Solving Autogenous Shrinkage to Reduce Emissions
Brucite consists of polar bound layers of ionically bound atoms
Strongly differentially charged surfaces and polar bound water account for many of the properties of brucite
Brucite hydrates consist of polar bound layers of ionically bound atoms
NB. We think this loosely bound polar water is available for the more complete hydration of PC.
In most concrete 18-23% of the PC used never hydrates. If all the PC used could be made to hydrate less could be used saving on emissions be around 20%.
2C3S+7H => C3S2H4 + 3CH
2C2S+5H => C3S2H4 + CH

## Slide 61: Economics of Tec-Cements
This embedded spreadsheet looks only at the binder price and assumes all other factors remain the same

## Slide 62: The Case for Manufactured Aggregates - Carbonates, Fly ash and other Wastes
Sand and stone aggregate are in short supply in some areas.
Nesquehonite is an ideal micro aggregate so why not agglomerate it and/or other magnesium carbonates to make man made manufactured aggregate?
Mg -> High molar volume growth
Ideal microstructure
Bonding
Stability
Ideal pH for wastes immobilisation
Sequestration
MgO binders will be suitable for this purpose and TecEco are seeking funding to demonstrate the technology.
TecEco can already agglomerate fly ash and nesquehonite without additional energy. We just can’t tell you how as we have not had the money to pursue a patent.

## Slide 63: Modified PC 50% Ternary PC Mix with N-Mg Route Mg Carbonate Aggregate
Chart: 
Assumptions - 50% non PC N-Mg mix and Substitution by Mg Carbonate Aggregate |  | 
Percentage by Weight of Cement in Concrete | 15.00% | 
Percentage by weight of MgO in cement | 6% | 
Percentage by weight CaO in cement | 29% | 
Proportion Cement Flyash and/or GBFS | 50% | 
1 tonne Portland Cement | 0.864 | Tonnes CO2
Proportion Concrete that is Aggregate | 72.5% | 
CO2 captured in 1 tonne aggregate | 1.092 | Tonnes CO2
CO2 captured in 1 tonne MgO (N-Mg route) | 2.146 | Tonnes CO2
CO2 captured in 1 tonne CaO (in PC) | 0.785 | Tonnes CO2
The addition of 6 - 10% MgO replacing PC in high substitution mixes accelerates setting.

## Slide 64: The Case for Manufactured Aggregates - Carbonates, Fly ash and other Wastes
Chart: 
Assumptions - 50% non PC N-Mg mix and Substitution by Mg Carbonate Aggregate |  | 
Percentage by Weight of Cement in Concrete | 15.00% | 
Percentage by weight of MgO in cement | 6% | 
Percentage by weight CaO in cement | 29% | 
Proportion Cement Flyash and/or GBFS | 50% | 
1 tonne Portland Cement | 0.864 | Tonnes CO2
Proportion Concrete that is Aggregate | 72.5% | 
CO2 captured in 1 tonne aggregate | 1.092 | Tonnes CO2
CO2 captured in 1 tonne MgO (N-Mg route) | 2.146 | Tonnes CO2
CO2 captured in 1 tonne CaO (in PC) | 0.785 | Tonnes CO2
With carbon trading think of the money to be made making man made carbonate aggregate
Source USGS: Cement Pages

## Slide 65: Modified PC 50% Ternary Mix with N-Mg Route Mg Carbonate Aggregate
25-30% improvement in strength
Fast first set
Better Rheology
Less shrinkage – less cracking
Less bleeding
Long term durability
Solve autogenous shrinkage?
Criteria | Good | Bad
Energy Requirements and Chemical Releases, Reabsorption (Sequestration?) | Use >50% replacements and still set like “normal” concrete! | 
Speed and Ease of Implementation | Rapid adoption possible | 
Barriers to Deployment |  | Permissions and rewards systems see http://www.tececo.com/sustainability.permissions_rewards.php
Cost/Benefit | Excellent until fly ash runs out! | 
Use of Wastes? or Allow Use of Wastes? | Uses GBFS and fly ash and nanufactured nesquehonite based aggregate | 
Performance |  | 
Engineering | Excellent all round | 
Thermal | High thermal capacity | 
Architectural | Excellent | 
Safety | No issues | 
Audience 1 |  | 
Audience 2 |  | 

## Slide 66: UTAS Testing - Rheology
Comment | Suggested Test | Possible Standard
Mixtures with high fly ash tend to be very sticky. My experience is that adding GBFS tends to fix this but MgO really makes the mix very creamy, slippery and easy to finish. | The aim is to obtain the parameters to describe a rheological model e.g Bingham plastic or Herschel-Bulkley . Use of a rheometer would be best if one is available. See http://ciks.cbt.nist.gov/~garbocz/rheologyNISTIR/ Otherwise the modified slump test (see paper/presentations attached) or J or U tube would give some ideas You may have some other apparatus. I agree with Ken Day, Ferraris and de Larrard that a lot could be learned from the torque on a mixer! | In spite of its well-documented limitations, the slump test has remained the default standard in the concrete industry. AS 1012.3.1-1998 We are looking for simple tests like the T500 and inverted cone tests

## Slide 67: Utas Testing – Rate of Early Setting
Comment | Suggested Test | Possible Standard
With high replacement the rate of setting so that finishing can occur is a problem and finishers/builders do not as a consequence like high replacement mixes. Preliminary work with modified ternary mixes suggests this has been overcome | A vicat needle (“penetration plunger”) is probably the way to go re first and final set. | AS 1012.18-1996 - Determination of setting time of fresh concrete, mortar and grout by penetration resistance.

## Slide 68: Utas - Shrinkage
Comment | Suggested Test | Possible Standard
Shrinkage is an issue with most mixes and both plastic and drying shrinkage are strongly reduced using MgO. There is less shrinkage with more added. | Suggest place strain gauges as soon as strong enough – 24 hrs ? Early shrinkage should be much less. From 7 days on can also be measured according to the standard. | AS 1012.13-1992 - Determination of the drying shrinkage of concrete for samples prepared in the field or in the laboratory (and AS 1012.13-1992/Amdt 1-1993)

## Slide 69: Utas Testing - Creep
Comment | Suggested Test | Possible Standard
The Chinese with their system think there is more creep. We have yet to demonstrate this in our system. This is probably a good thing as concrete is too brittle. |  | AS 1012.16-1996 - Determination of setting time of fresh concrete, mortar and grout by penetration resistance

## Slide 70: UTas Testing – Split Tensile & Modulus of Elasticity
Comment | Suggested Test | Possible Standard
We have done some testing and found the split tensile strength greater. Confirmation would be useful. |  | AS 1012.10-2000 - Determination of indirect tensile strength of concrete cylinders (Brasil or splitting test)
Hopefully not too much higher |  | AS 1012.17-1997 - Determination of the static chord modulus of elasticity and Poisson's ratio of concrete specimens

## Slide 71: Utas Testing – Autogenous Shrinkage
Comment | Suggested Test | Possible Standard
Because brucite initially forms brucite hydrates we believe we have solved two issues in concrete which are incomplete hydration of PC and autogenous shrinkage particularly in high strength concretes. We strongly suspect that the polar bound hydrate water becomes available for more complete hydratation of PC, improving the MPa/PC ratio and reducing autogenous shrinkage. | I want to test this at various temperatures See Du, C. (2005). "A Review of Magnesium Oxide in Concrete - A serendipitous discovery leads to new concrete for dam construction." Concrete International (December 2005): 45 - 50. I think some differential semi quantitative XRD would also be useful to determine the proportion of un hydrated cement in samples. No or low un hydrated cement after say 180 days means less cement for the same strength and no autogenous shrinkage | 

## Slide 72: Utas Testing – Durability Issues
Perceived Problem | Comment | Suggested Test | Possible Standard
Flexural Strength | It is important to get some idea of the modulus of rupture. |  | AS 1012.11-2000 – Determination of the modulus of rupture
Density | We have had reports of increased and decreased density so we would be interested in your result. |  | AS 1012.12.1-1998 – Rapid method AS 1012.12.2-1998 – Water displacement method
Chloride and Sulfate in Concrete | Free chloride and sulphate in cement is an issue with the dry process of manufacturing cement. MgO should bind these unwanted elements rendering them non mobile and harmless. |  | AS 1012.20-1992 - Determination of chloride and sulfate in hardened concrete and concrete aggregates

## Slide 73: Utas Testing – Durability Issues
Perceived Problem | Comment | Suggested Test | Possible Standard
Chloride Penetration | Chloride penetration is an issue in aggressive environments. We think we should reduce this because of the formation of oxychlorides |  | The Nordtest NT BUILD 443, 1995 is a standard method for evaluation of the chloride diffusion coefficient of concrete by accelerated laboratory testing.
Sulphate Resistance | Chloride penetration is an issue in aggressive environments. We think we should reduce this because of the formation of oxysulphates |  | Potential expansion of concrete in sulphate environments should be assessed in accordance with AS2350.14 by immersing mortar samples (sieved out of each concrete or made separately with no stone) in a sulphate solution for over 16 weeks.

## Slide 74: Anthropogenic Sequestration Using Gaia Engineering will Modify the Carbon Cycle
Photosynthesis by plants and algae
Consumed by heterotrophs (mainly animals)
Organic compounds made by autotrophs
Organic compounds made by heterotrophs
Cellular Respiration
Cellular Respiration burning and decay
Limestone coal and oil burning
Gaia Engineering, (Man made carbonate, N-Mg Process,TecEco Kiln and Eco-Cements)
Decay by fungi and bacteria
CO2 in the air and water
More about Gaia Engineering at
http://www.tececo.com.au/simple.gaiaengineering_summary.php